Nature-inspired and sustainable synthesis of sulfur-bearing Fe-rich nanoparticles

David O’Connor1, Deyi Hou1*, Qingsong Liu2 Martin R. Palmer3, Rajender S. Varma 4*

1 School of Environment, Tsinghua University, Beijing 100084, China

2 Department of Ocean Science and Engineering, Southern University of Science and Technology, Shenzhen, 518055, China

3 School of Ocean and Earth Science, University of Southampton, Waterfront Campus, Southampton, SO14 3ZH, UK

4 Regional Centre of Advanced Technologies and Materials, Faculty of Science, Palacky University, Šlechtitelů 27, 783 71 Olomouc, Czech Republic.

* corresponding author (hou.deyi@tsinghua.edu.cn)

Abstract. Sulfur-bearing Fe-rich nanoparticles (SINPs) have been subject to increased levels of interest because of their catalytic properties and other features. However, with increasing interest in greener and sustainable practice, traditional engineered routes to SINP synthesis have become a concern owing to their high energy and resource demand as well as the use of potentially hazardous or environmentally harmful reagents.  Here, we aim to bring attention to emerging and burgeoning research across a wide range of disciplines on the formation of both naturally occurring and synthetic SINPs. Firstly, various SINP types are described, and their most important characteristics are outlined. Second, the natural mechanisms of SINP formation are evaluated and their environmental significance explained, predominantly in hydrothermal vents and lithogenic environments, in order to help inspire new approaches to engineered synthesis. Third, an appraisal of various synthetic approaches for SINP assembly is presented, with a focus on green synthesis methods. One exemplar is the use of nature-inspired biosynthesis, which has been increasingly explored for the fabrication of cost-effective and environmentally friendlier SINPs. Finally, potential future research directions leading to more sustainable SINP synthesis are put forward.

Keywords: nanostructures; nanomaterial fabrication; green synthesis; biosynthesis; iron sulfides

Abstract Graphic:

Synopsis. An appraisal of various natural and synthetic mechanisms for SINP formation with a focus on greener synthetic approaches

# List of Abbreviations

AAO		anodic aluminum oxide

CMC		carboxymethyl cellulose

CVD		chemical vapor deposition

IDP 		interplanetary dust particle

IRB		iron-reducing bacteria

LIB 		lithium-ion battery

Ms 		saturation magnetization

MTB 		magnetotactic bacteria

NPs		nanoparticles

PV 		photovoltaic

SDS		sodium dodecyl sulfate

SINPS		sulfur-bearing iron-rich nanoparticles

SRB		sulfur-reducing bacteria

TEM		transmission electron microscopy

ZVI 		zero valent iron

# Table of Content

# Introduction

The International Organization for Standardization (ISO) define nanoparticles (NPs) as particles with dimensions that do not exceed 100 nm 1.  These particles possess physical and chemical properties that differ from bulk materials; for example, they may display exceedingly high surface area-to-volume ratios, quantum effects, and semi-conductor band gaps relating to their dimensions 2. Thus, the application of NPs benefits many technologies and consumer products, including renewable energy technologies, personal care products, biomedicines, agrochemicals and water/soil environmental treatment processes 3-5.

An expanding body of research pertaining to sulfur-bearing iron-rich nanoparticles (SINPs) has been of prime interest due to their utility in catalytic, electromagnetic, and optical applications, and because of the natural abundance of SINP precursor material resources 6-9. However, sustainability concerns persist regarding SINP manufacturing, including the associated environmental impacts and the desire to reduce production costs 10. This has led to growing interest in the adoption of sustainable materials and green technological approaches 11.

Based on research that extends across a wide range of disciplines and includes both naturally occurring and synthetic nanomaterials, researchers are increasingly generating innovative solutions to improve synthesis sustainability 12. For example, the emerging ‘nature-inspired’ design philosophy is based on copying natural formation mechanisms 13. Such approaches have been particularly important in the development of improved synthesis methods associated with low secondary impacts 14, 15.

Herein, we examine both natural and engineered synthesis of SINPs in an attempt to provide an improved understanding of the formation of this class of NP and encourage the development of more sustainable SINP synthesis techniques. The structure of this paper reflects the objectives of the review undertaken, which are as follows: (1) to review the various SINP types and outline their most important characteristics; (2) to evaluate the natural formation of SINPs, with the natural mechanisms of SINP formation and their environmental significance explained in order to encourage researchers to develop new nature-inspired synthesis processes; and (3) to provide an appraisal of various synthetic approaches for SINP assembly, with a focus on green synthesis methods. Finally, suggested future research directions for the advancement of more sustainable SINP synthesis techniques are provided.

# Types and characteristics of sulfur-bearing Fe-rich nanoparticles

Different types of SINPs, which comprise various iron-sulfide compounds, have received attention in recent years because of their characteristics; including their optical absorption coefficients and photovoltaic (PV) conversion efficiencies 16-18.  In this section, various SINP types and their characteristics are outlined, which is briefly summarized in Table 1 for reference.

Table 1 Summary of the types and characteristics of sulfur-bearing iron nanoparticles (SINPs)

| SINP Type | Characteristics |
| --- | --- |
| FeS, mackinawite and troilite (approximate FeS) | Iron(II)sulfide (FeS) is not normally stable in an amorphous form, cubic FeSc has a cubic F43m structure and is not found in nature because it easily converts to mackinawite 19, 20. Mackinawite, expressed in the formula FeSm, comprises Fe atoms surrounded by four sulfur atoms in a nearly perfect tetrahedron structure, 21 forming a tetragonal P4/nmm structure 19. It is a widespread metastable mineral in low-temperature environments. FeS can also be found in nature as troilite (FeSt), a near stoichiometric iron sulfide with a hexagonal P62c structure 19. It is the stoichiometric end member of the pyrrhotite mineral group having antiferromagnetic properties at ambient temperature 22. |
| Pyrrhotite (Fe1-xS) | Pyrrhotite (Fe1-xS where x = 0 to 0.13) minerals are non-stoichimetric variants of FeS which exist as monoclinic (e.g., A2/a) or hexagonal (e.g., P6/mmc) structures, 19 or trigonal phases 23. It is the ordered omission of Fe that produces superstructures that range from hexagonal to monoclinic 24. The monoclinic structure (often denoted as Fe7S8, but with a wide compositional range) contains alternating layers of full iron sites and layers of sites with iron vacancies. Pyrrhotite with a hexagonal structure (i.e., the nickel arsenide (NiAs) structure) will distort into a monoclinic structure if the vacancy content is greater than 0.11 per formula unit 25. Hexagonal primary pyrrhotite can be partially oxidized when exposed to oxygen, forming iron deficient secondary pyrrhotite 23. |
| Greigite (Fe3S4) | Greigite (Fe3S4) has a cubic Fd3m structure 19, and is the iron sulfide counterpart of spinel magnetite (Fe3O4,), although greigite is a normal metal whereas magnetite is only half-metallic 26. The unit cell of the stoichiometric inverse spinel greigite structure contains 32 sulfur atoms and 24 iron atoms 27, 28, with two sub-lattices of iron atoms with Fe3+ ions occupying tetrahedral A-sites and Fe2+ and Fe3+ ions occupying octahedral B-sites 29. While greigite is thermally stable at ambient temperature, it will break down to form pyrrhotite when heated, and slowly dissolves in hydrofluoric acid or warm hydrochloric acid 27. The relative instability of greigite has resulted in it being less well studied than magnetite, but engineered greigite is now receiving greater interest owing to its complex magnetic properties 30. |
| Pyrite (FeS2) | Pyrite has the composition of FeS2p and forms in a cubic Pa3 structure 19. It is one of the most abundant minerals of the Earth’s surface. |

## FeS, mackinawite and troilite (approximate FeS)

Iron(II)sulfide (FeS) is not normally stable in its amorphous form. Cubic FeSc has a cubic F43m structure and is not found in nature 19, because it readily converts to mackinawite 20.  Mackinawite, expressed in the formula FeSm, comprises Fe atoms surrounded by four sulfur atoms in a nearly perfect tetrahedron structure, 21 forming a tetragonal P4/nmm structure 19.  It is a widespread metastable mineral in low-temperature aqueous environments, being the major FeS constituent precipitated from aqueous solutions 31. In terms of its technological applications, mackinawite has seen much interest in environmental technology as a reducing reagent (e.g., for the dechlorination of chlorinated organic pollutants) and sorbent for divalent metals 32.

FeS can also be found in nature as troilite (FeSt), with a hexagonal P62c structure 19.  It is the stoichiometric end member of the pyrrhotite mineral group,  having antiferromagnetic properties at ambient temperature 22.  Troilite forms in nature under strongly reducing environments, and is less abundant in terrestrial environments than other pyrrhotite minerals, being only found at low concentrations where there are strongly reducing environments 23.  However, troilite is abundant in meteorites, and it may occur in massive forms (up to 5 cm crystals) in iron meteorites 23.  A characteristic of troilite is that when is heated to above the β-transition temperature (315 °C), it is transformed from an antiferromagnetic structure to a paramagnetic structure with magnetic moment disordering (Fig. 1), which is accompanied by a phase transformation to the NiAs subcell (1C) 23.

Fig. 1 Heating-induced transition of the magnetic moment configuration in troilite (adapted from Wang and Salveson (2005) 23 with permission)

## Pyrrhotite (Fe1-xS)

Pyrrhotite (Fe1-xS where x = 0 to 0.13) minerals are non-stoichimetric variants of FeS which exist as monoclinic (e.g., A2/a) or hexagonal (e.g., P6/mmc) structures, 19 or trigonal phases 23. Pyrrhotite minerals are relatively abundant on Earth, being found in many geological settings 19.

It is the ordered omission of Fe that produces superstructures that range from hexagonal to monoclinic 24.  The monoclinic structure (often denoted as Fe7S8, but with a wide compositional range) contains alternating layers of full iron sites and layers of sites with iron vacancies.  Pyrrhotite with a hexagonal structure (i.e., the nickel arsenide (NiAs) structure) will distort into a monoclinic structure if the vacancy content is greater than 0.11 per formula unit 25.  The hexagonal form of Fe7S8 is stable and antiferromagnetic, whereas monoclinic pyrrhotite is strongly ferrimagnetic.  Hexagonal pyrrhotite is known to naturally form in many geological settings, including deep-sea sediments associated with methane hydrates  33.  Hexagonal primary pyrrhotite can be partially oxidized when exposed to oxygen, forming iron deficient secondary pyrrhotite 23. Monoclinic pyrrhotite exists widely in reduced igneous rock and metamorphic rocks and can be transported to marine sediments as an erosional product. Once it is present in marine sediments, monoclinic pyrrhotite is an excellent provenance tracer. Notably, it is particularly common in extra-terrestrial rocks 34.

Because numerous pyrrhotite superstructures occur with varying iron vacancy arrangements, 35 they display various magnetic and electrical properties 36-38.  For instance, pyrrhotite minerals display a range of thermomagnetic behaviors depending on the precise composition 25.  The pyrrhotite Curie temperature is reported as 310~325 °C depending on the composition, and is considered stable and ferrimagnetic at lower temperatures 25.  Impurities as an isomorph substitute (e.g., incorporation of Ni) can significantly lower the Curie temperature value.  When pyrrhotite is heated to >325 oC, the magnetic moment decreases dramatically, due to long-range magnetic moment disordering or vacancy disordering confined to different sites in alternating rows in each vacancy layer 29.  The structures of other Fe1-xS variants have partially filled Kagome net layers and Fe-filled layers stacked with long-range orders established along the c axis 39.  Several other pyrrhotite minerals such as Fe9S10, Fe10S11, and Fe11S12, are generally hexagonal, antiferromagnetic, and only stable at temperatures below 209 °C 40.

## Greigite (Fe3S4)

Greigite (Fe3S4) has a cubic Fd3m structure 19, and is the iron sulfide counterpart of spinel magnetite (Fe3O4,), although electronic structure calculations show that greigite is a normal metal whereas magnetite is only half-metallic 26. Greigite was first observed in clay layers, as grains and crystals, in drill cores retrieved in San Bernardino, California, USA 27, but it is now know to be widespread in the natural environment, being mostly associated with fresh water systems, where it can be stable for millions of years 41.  Aquatic magnetotactic bacteria (MTB) have also been found to contain greigite, which they utilize to migrate along geomagnetic field lines 42.

The unit cell of the stoichiometric inverse spinel greigite structure contains 32 sulfur atoms and 24 iron atoms 27, 28, with two sub-lattices of iron atoms with Fe3+ ions occupying tetrahedral A-sites and Fe2+ and Fe3+ ions occupying octahedral B-sites 29.  While greigite is thermally stable at ambient temperature, it will break down to form pyrrhotite when heated, and slowly dissolves in hydrofluoric acid or warm hydrochloric acid 27.  The relative instability of greigite has resulted in it being less well studied than magnetite, but engineered greigite is now receiving greater interest owing to its complex magnetic properties 30.

Band structure calculations have revealed a complex Fermi surface and the influence of relativistic effects.  For example, two sheets of the Fermi surface disappear or reappear depending on the direction of applied magnetization.  This phenomenon enables spintronic engineering at a single compound level, an advancement over traditional heterostructures 26.  However, the magnetic properties of engineered greigite are sensitive to synthesis conditions, and knowledge of these properties is incomplete 43.  It is also difficult to synthesize pure greigite because most methods will also produce other iron sulfide impurities, such as mackinawite and pyrite 44. This is usually discovered by observing X-ray diffraction patterns, which often reveal non-greigite peaks. Nevertheless, pure synthetic greigite has been extensively investigated by a series studies by Chang and his colleagues 45-48

For bulk greigite, the expected saturation magnetization (Ms) at room temperature is 4 μB per formula unit (f.u.), however, Ms values are usually measured to be < 2.5 μB/f.u., implying poor purity (i.e., mackinawite and pyrite impurities, see above) 49. The parameter of exchange interaction (JAB) between Fe ions in (A) and (B) sub-lattices is estimated at 1.03 meV, and no low temperature magnetic transition is present 29.

Greigite SINPs have potential to be used as an anode material in lithium-ion batteries (LIBs) 50, and as intermediates in solar cells 44.  Interest in the use of greigite in LIBs has been increasing because of its high theoretical capacity of 785 mAh/g, which is more than twice that of conventional graphite (372 mAh/g) 49.   It is also noteworthy that greigite is non-toxic and abundant on Earth. Furthermore, greigite SINPs hold potential applications in the areas of hydrogen storage, magnetic guided delivery of drugs, and for cancer hyperthermia applications 51, 52.  Greigite NPs have also been used as an enzyme mimetic to catalyze chemical reactions because natural enzymes are vulnerable to changing acidity, temperature, and inhibitors 53.  The intrinsic enzyme mimetic activity is similar to natural peroxidases and has been exploited to develop novel immunoassay methods. Greigite has a stronger affinity than Fe3O4 in peroxidase-like behavior, which suggests that greigite SINPs have good potential for medical detection applications 53.

## Pyrite (FeS2)

Pyrite has the composition FeS2p, forms in a cubic Pa3 structure, and is one of the most abundant minerals of the Earth’s surface 19 (FeS2 with an orthorhombic crystalline structure is known as marcasite). Pyrite has many uses for modern technological processes. For example, its high adsorption coefficient (α >105 cm-1 for hv >1.3 eV) and band gap (0.8~0.95 eV) make it useful as an PV absorber material 22, 54, 55.  Pyrite-containing devices have high quantum efficiency (>90%), high photocurrents (>40 mA cm-2), and low photo-voltages (<200 mV) 56-58.  Pyrite nanocrystals can also be deposited on flexible substrates such as solar ink or paint in order to provide large surface area PVs 59.  Importantly, cobalt can also be substituted in cubic pyrite nanocrystals (CoxFe1−xS2) as nanoscale thin films, to enable switching from p-type to n-type semi-conductors between x=0.16 and x=0.21 60. Compared to traditional single crystal pyrite, pyrite NPs offer a cost-effective and highly scalable options for such applications.  As a PV material, pyrite NPs have the benefit of wide natural abundance and relatively low toxicity to humans.  Moreover, if some of the vast amounts of pyrite discarded as a mining waste could be captured for use in solar PV and photo-electrochemical cells 54, it would not only be a waste-to-resource gain, but also help reduce the impacts of acid mine drainage caused by pyrite oxidation.

Other promising uses for pyrite SINPs are in high-performance cathodes for energy storage, e.g. lithium-ion batteries (LIBs), due to their long shelf life and relatively high capacity, 55 and in wastewater treatment due to its high catalytic activity toward organic pollutants. For example, Pyrite SINPs show high photo-catalytic activity towards organic dyes (e.g., methylene blue and Synazol Yellow K-HL), due to the creation of reactive oxygen species via a photo Fenton like process 61.

## Multi-metallic SINPs

Multi-metallic SINPs have been explored to address issues arising among the various SINP types.  For example, while pyrite has great potential as a PV material, due to its high adsorption coefficient and band gap, it also suffers from crystal defects arising from sulfur vacancies 62, 63, which may be mitigated by the use of  bimetallic pyrite.

Naturally occurring bimetallic FeS minerals are also found in sedimentary, hydrothermal, and igneous environments.  For instance, arsenic can be incorporated into iron-sulfide as arsenian pyrite (referred to as arseno-pyrite) in the form of As3+-pyrite (As substitute for Fe) or As1--pyrite (As substitute for S) 64.  Arsenian pyrite is an important host of gold in hydrothermal ore deposits, as well as a source of arsenic pollution in the natural environment 65, 66.  While As3+-pyrite tends to form under oxidizing conditions, As1--pyrite will form under relatively reducing conditions.  As3+-pyrite formation on pure pyrite depends on the crystal size, with larger crystal sizes containing higher arsenic concentrations 64.

Other bimetallic iron sulfide minerals found in nature include pentlandite ([Fe,Ni]9S8), which is a common mineral in chondritic meteorites, polar micrometeorites, and chondritic interplanetary dust particles (IDPs) 67. Bimetallic CuFeS2, which is found in volcanogenic massive sulfide deposits among other environments 68, may offer greatly increased efficiency in the conversion of waste heat into energy. For example, synthetic ~6.4 nm bimetallic CuFeS2 can display thermoelectric values ~77 times higher than bulk chalcopyrite 69.

## Core-shell SINPs

Various core-shell SINPs have been developed and synthesized for various technological applications.  For example, core-shell Au/FeS NPs with polyethylene glycol coatings have been developed  in which the Au component functions as a radiosensitizer in medical applications 70.  The FeS component of these SINPs provides contrast to enhance magnetic resonance imaging and photoacoustic imaging, and the coating enables higher dosages without the associated metal toxicity to patients.

In environmental applications, methods have been developed for large-scale synthesis of core-shell FeS NPs, involving FeS shells on zero valent iron (ZVI) NPs 71, 72.

# Formation of SINPs in natural environments

Natural Sulfur-bearing Fe species occur in many natural environments, with iron sulfides being among the most extensively dispersed reduced S species found on Earth. For example, sulfur-bearing Fe-rich minerals are a common constituent of the lithosphere, being found in many types of geological bodies, such as ancient sedimentary rocks, modern sediments, mineral deposits, and submarine hydrothermal vent deposits. As well as the lithosphere, naturally formed NPs have also been discovered in the troposphere (and even higher), the hydrosphere (oceans, lakes, rivers, and groundwater), and the biosphere (principally microbes, but also in higher organisms including humans) 73, and even on asteroids 74.  In this section we explore these naturally forming S-bearing Fe-rich NPs in order to provide inspiration for the development of new engineered synthesis techniques.

## Lithosphere

Sulfur-iron reactions play key roles in the geochemistry of the lithosphere, from low-temperature (<100 oC) sedimentary systems 75, 76, intermediate-temperature (100-400 oC) hydrothermal sulfide deposits that form large ore bodies 77, to high temperature (up to 1000 oC) igneous and metamorphic rocks 78. While SINP formation has not been reported as primary phases in high-temperature rocks,  SINPs may form in low- to intermediate-temperature systems by a variety of processes; including dissolution-precipitation reactions or via mechanical breakdown of bulk iron sulfides and other weathering processes 11, 73.  The volumetrically most important Fe-S minerals in these settings are pyrite, mackinawite and greigite.

In natural lithogenic reactions (Fig. 2), Fe2+ is released into solution by the dissolution of Fe bearing minerals (i.e., ferric (hydr)oxides) under reducing conditions, which occurs largely by microbe facilitated dissimilatory Fe reduction, or by abiotic reactions involving dissolved reductants 79. In reducing conditions, sulfur will tend to exist as sulfide (i.e., HS- at pH > 7). The reduction of sulphate to sulfide is also commonly biologically mediated, although it may also occur by interaction with reduced iron species. H2S is a slightly soluble microbial product that acts as a weak acid, yielding HS− (pKa = 6.9) and S2− (pKa = 11.96).

Fig. 2 Pathway to pyrite formation (adapted from Berner (1984) 80 with permission)

A variety of SINPs can form via dissolution-precipitation reactions, including mackinawite (FeS) as a nano crystalline or amorphous phase 81-83. FeS species may react with dissolved polysulfides to form pyrite 79, via microbial formation of mackinawite on iron oxide particles 84. High-resolution transmission electron microscopy (TEM) observations of materials isolated from marine sediments have revealed mackinawite nano-crystalline structures containing 10-15 atomic layers 85.

During diagenesis, greigite will grow if dissolved Fe and S2 are available. Its formation and preservation rely on various factors including the availability of organic carbon, S2 production, and presence of reactive Fe 43. Greigite is a precursor in the Fe–S system to pyrite formation (Fig. 2)  80, 86, 87.  Natural incorporation of trace elements/impurities into natural SINP structures can occur in a range of low- to intermediate-temperature environments 65, 88-90.  Of these, one of the most notable involves the incorporation of As, either by substitution of As-1 for S in the sulfide unit of pyrite (thus forming arsenopyrite, Fe(As,S)2) or, under non-equilibrium kinetically controlled environmental conditions, As3+ can also be incorporated into pyrite, by substituting for Fe2+ 64.

## Microbial processes

In oxygen absent environments, anaerobic bacteria use alternatives to oxygen as electron acceptors.  Sulfate-reducing bacteria (SRB), which are ubiquitous in anaerobic water columns and sub-aqueous sedimentary environments, play a key role in iron-sulfur mineralization in sedimentary environments, including the formation of mackinawite, pyrite, and greigite.  The initial step in the formation of bulk iron sulfide minerals involves the formation of SINPs, with the cell wall being coated with nano-sized iron-sulfide precipitates (Fig. 3).

Fig. 3 Transmission electron microscopy (TEM) image of the cell of a sulfate-reducing bacterium (SRB) coated with nano-sized iron-sulfide precipitates (reproduced from Watson et al. (2000) 91 with permission)

Dissimilatory metal-reducing bacteria can respire elemental sulfur (S0) as an alternative electron acceptor in alkaline pH environments, leading to mackinawite formation in alkaline groundwater systems. In this case, microbial and abiotic processes are coupled. For example, sulfur reduction by SRB leads to iron(III) reduction by an abiotic reaction with sulfide, which, in turn, leads to further sulfur reduction by SRB 92. Thus, sulfur is recycled for multiple rounds of SRB reduction (see Fig. 4).

Fig. 4 Dissimilatory metal-reducing bacteria can respire elemental sulfur (S0) as an alternative electron acceptor in alkaline pH aquifer environments leading to mackinawite formation. Microbial (green) and abiotic processes (black) are coupled together (adapted from Friedrich and Finster (2014) 92 with permission)

In experiments conducted at pH 7, nanoscale mackinawite rims have been observed on lepidocrocite crystals, with interfacial magnetite forming as a steady state layer as a product of lepidocrocite-mackinawite interaction. During the initial stages of these reactions, Fe2+ forms in excess to FeS. The fraction of excess Fe2+ increases at lower sulfide to surface site ratios, suggesting kinetic decoupling of sulfide oxidation and Fe2+ detachment from lepidocrocite. This may be due to sulfide donating electrons to lepidocrocite at a faster rate than stoichiometric amounts of FeS production.  After 2 days of experimental observation, Fe2+ and S0 levels decreased, resulting in pyrite formation dislocated from the lepidocrocite surface, as well as traces of magnetite.  The absence of dissolved sulfide under these conditions suggests the formation of polysulphides, which are precursors for pyrite formation 84.

In addition to SRB, iron-reducing bacteria (IRB) play an important role in SINP formation. For example, IRB in acid mine drainage facilitate iron sulfide formation under anoxic conditions 93.  Again, this observation may aid in devising a biosynthesis method for SINP production. Magnetotactic bacteria (MTB) facilitate the formation of nanoscale ferrimagnetic greigite (Fe3S4), mackinawite (tetragonal FeS) and, tentatively, cubic FeS 20.  The mackinawite converts to greigite within the MTB by rearrangement of the Fe atoms, hence MTB are responsible for magnetic SINPs production in some sediments 91, 94.  MTB also produce magnetosomes containing single-domain magnetite particles or single-domain greigite particles.

It should be noted that there can be notable divergence in the characteristics between different types of bacterially formed SINPs. For instance, SRB produced SINPs that possess a strong adsorption potential for a wide range of metal ions involve the inclusion of materials not normally precipitated as sulfides, while SINPs produced within magnetosomes are relatively pure 91. The great diversity of microbes in natural systems means that their role in formation of SINPs under a wide range of conditions is far from fully understood.  For example, it has been observed that Thiobacillus denitrificans can oxidize pyrite SINPs to Fe3+ and SO4-2 in the presence of NO3- 95, whereas samples lacking Thiobacillus denitrificans showed no oxidation effects.  A key factor in this oxidation process is the nanoscale size of the pyrite SINPs, with this fraction being preferentially oxidized, whereas larger pyrite crystals remained intact.  This suggests a significantly higher bioavailability of nano-particulate minerals compared to larger mineral phases.

## Submarine hydrothermal vents

High temperature submarine hydrothermal vents are key sources of oceanic Fe 96.  Although much of the Fe that initially emerges from the vent orifice is in the form of dissolved Fe2+, as the >300oC reduced fluids cool and mix with oxidized ambient seawater, the Fe rapidly oxidizes and a proportion of the dissolved Fe precipitates as Fe(OH)3.  Because hydrothermal fluids also contain high concentrations of dissolved reduced S, polymetallic sulfides also precipitate (including nano-sized particles) as the vent fluid cools.  Indeed, as much as 10% of total Fe emitted by vent fluids may consist of SINPs 97.  In addition, pyrite SINPs (<200 nm) can form within the high temperature–pressure environment of an up flow zone of hydrothermal vents, before discharging to the ocean 97.  Overall, hydrothermal vent-derived SINPs vary in shape and size, with typical aggregate diameters of 50-350 nm 98.  Hence, while coarser and denser particles settle to the seabed within the immediate vicinity of the vent site, finer grained particles may be carried by buoyant hydrothermal plumes (Fig. 5) 97, 99, 100.  They may then be transported for 100’s to 1000’s km by bottom water currents 99.

Fig. 5 Formation of pyrite SINPs in deep ocean hydrothermal environments. Vent iron may exist in various forms including pyrite (FeS2) SINPs. By remaining in suspension, pyrite SINPs are able to evade mass precipitation zones rising 1~5 m above hydrothermal vents (adapted from Yucel et al., (2011) 97 with permission)

Laboratory experiments have suggested that the stable dispersion of hydrothermally-generated SINPs is aided by the slower oxidation kinetics (by several orders of magnitude) of pyrite SINPs relative to coarser-grained materials 100. In mimicking hydrothermal vent conditions, engineered SINPs have been manufactured in the laboratory by heating dissolved Fe and H2S together at 140 oC, followed by rapid quenching at 0 oC 98.  It is notable that the experimental studies incorporating powdered SiO2 in the reaction mixture yielded SINPs that were closest in mineralogy and morphology to those found at hydrothermal vents.  It has been suggested that this is because the silica particle surfaces create a favorable environment for pyrite nucleation, and it is noteworthy that both dissolved and particulate SiO2 are major components of submarine hydrothermal systems 98.

## Paleoenvironmental role

On the tectonic time scale, global sulfur and carbon cycles are well coupled, and thus provide important environments for biological activities. Formation of pyrite via bacterial sulfate reduction can result in very negative δ34S values owing to preferential utilization of 32S by SRB. Studies have revealed large changes in δ34S values over the last 550 Ma. Such long-term variations could be due to pyrite burial in the sedimentary reservoir 101, 102. In contrast, short-term variations in δ34S values could relate to vertical heterogeneity (e.g., ocean stratification) 103.

Naturally formed greigite plays a role of interest in paleomagnetic and environmental magnetic studies 77, 104-106. On an orbital timescale, the formation and preservation of greigite can be modulated by ocean ventilation and variations in redox conditions caused by sea level changes. For example, sedimentary cores extruded from the South China Sea have revealed that fine-grained greigite dominated during glacial periods under anoxic conditions owing to disconnection between the South China Sea and the Indian Ocean 107. In contrast, ventilation becomes rigorous during glacial periods and coarser-grained detrital (titano) magnetites are prevalent.

Continental shelves bridge the continent and ocean. Sediments in these regions are sensitive to sea-level variation, with redox conditions changing rapidly with respect to the fast sea level changes. This can cause thick layers of greigite to occur. For example, a thick (~8 m) laterally distributed layer of greigite occurred during the marine isotope stages 17-13 within the scope of the Yellow Sea Warm Current from the Chinese Yellow sea 108.  The occurrence of greigite corresponds to enrichment by the trace element cadmium (Cd), which indicates that a weak sulfidic condition was accomplished with trace levels of freely dissolved H2S. Studies have shown that Cd2+ has faster water exchange reaction kinetics than Fe2+, therefore, CdS precipitates prior to FeS formation and subsequent pyrite formation 109. CdS formation would consume a certain amount of S and cause weak sulfidic conditions. This seems to favor the formation of greigite rather than pyrite. Direct evidence has been put forward showing that Cd concentrations peak at the redox boundary rather than a full reductive environment 110.

## Environmental fate

Pyrite is the most abundant iron sulfide mineral in the lithosphere, yet its transformation in natural environments is not fully understood.  Iron sulfides may exist buried within anaerobic sediments and rocks for millions of years before they are transported to oxygenated submarine and subaerial environments, where they can be oxidized by nitrate, Fe(III) oxides, or MnO2 as electron acceptors 111.  These processes are sometimes exploited by the mining industry to produce copper from low-grade ores 112, but pyrite oxidation also generates potentially harmful sulfuric acid (e.g., acid mine drainage) 112.  In anoxic geological reservoirs, pyrite can be stable almost indefinitely 111, although ferric iron can oxidize pyrite 113, 114 and anaerobic pyrite oxidation by nitrate as an electron acceptor has been observed in natural sediments 115, 116.

There is much uncertainty regarding the environmental fate of SINPs and the full role that these NPs play within the natural environment, with physicochemical, macro-molecular, and biological pathways all contributing 117.  For example, hydroxyl radicals formed as products of FeS oxidation can lead to oxidation and increased mobility of toxic As 118.  SINPs also display higher reactivity in microbial processes compared to bulk materials.  For example, pyrite SINPs are readily oxidized to ferric iron and sulphate by microbial processes, with a closed recovery of electrons in pyrite oxidation and nitrate reduction reactions 95.

## Space weathering

The first sulfur-iron species formed in the early solar nebula is believed to be stoichiometric FeS (troilite) 119.  However, chondritic IDPs, which represent the earliest formed material available for study, contain abundant iron sulfides with more pyrrhotite than troilite. This suggests pyrrhotite to be an important nebular condensate phase caused by ‘space weathering’, which altered the troilite surface 120.  SINPs have also been found on extraterrestrial materials returned to Earth from the 25143 Itokawa asteroid 74.  In this case, surface alteration was discovered on half of the particles examined, with SINPs being present in 5 - 15 nm layers on surfaces of olivine, low-Ca pyroxene, and plagioclase. These likely stemmed from vapor deposition. Some SINPs embedded in the surface of the olivine substrates show lattice fringes not consistent with troilite and pyrrhotite, likely due to the presence of Mg accompanied by SINPs 74.

# Engineered SINP synthesis

A wide range of different synthesis procedures and approaches have been developed in recent years for the fabrication of engineered SINPs (Table 2). The main approaches include ‘bottom-up’ wet-chemistry or ‘top-down’ mechanical approaches, by which SINPs of different sizes, shapes, and compositions can be produced.  An outline of various synthesis approaches is provided in this section, but the reader should refer to the original publications for details of specific synthesis methods. It should be regarded that SINPs of certain stoichiometries are sometimes rather difficult to synthesize precisely due to the complexity of the Fe-S system phase diagram (Fig 6).

Table 2. Selected Sulfur-bearing Fe-rich nanoparticle synthesis procedures and approaches

| SINP Type | Synthesis method | Reference |
| --- | --- | --- |
| biochar supported FeS | FeSO4•7H2O was mixed with carboxymethyl cellulose (CMC) and biochar. Na2S solution was added dropwise to the solution | 121 |
| CdxZn1-xS@Fe3S4 | iron triacetylacetonate was dissolved in ethylene glycol solution. Thioacetamide was added and allowed to react for 2 h before Cd(NO3)2 and Zn(NO3)2 were added | 122 |
| CMC-stabilized FeS | CMC solution was mixed with FeSO4 and Na2S solutions | 123 |
| Fe/FeS | Fe and S powders were milled together, and heat treated at 1123 K | 124 |
| Fe3S4-C | FeCl3 and thioacetamide were dissolved in ethylene glycol and glucose added | 125 |
| FeS | FeSO4 aqueous solution was mixed with Na2S solution. Carboxymethyl cellulose (CMC) was added as a stabilizer | 126 |
| FeS | lactate was added as electron donor, with thiosulfate added as electron acceptor and sulfur source. Naphthol green B was also added | 127 |
| FeS coated ZVI | FeSO4 was mixed with NaBH4 and thioacetamide | 128 |
| FeS stabilized with biopolymers | biopolymers were extracted from basidiomycetous fungus (Itajahia sp.) | 129 |
| FeS/FeSe | trinuclear iron (III) precursor complex reaction with thiourea | 130 |
| FeS2 | FeCl2•4H2O was mixed with Na2S2O3 and heated at 200°C for 24 h | 61 |
| FeS2 | high energy mechanical ball milling | 131 |
| FeS2 | plasma-treated pyrite was prepared with an Ar glow discharge plasma | 132 |
| FeS2 | pyrite ore was treated with glow discharge plasma in a N2 atmosphere | 133 |
| FeS2 | reaction of FeSO4•7H2O with Na2S2O3•5H2O | 134 |
| FeS2 | FeCl2 and oleylamine were mixed, followed by sulfur injection and heating to 220 °C | 135 |
| magnetic FeS | biosynthesis with desulfovibrio vulgaris miyazaki | 136 |
| magnetic sulfide modified ZVI | sodium borohydride and dithionite were added to FeCl3 solution by titration | 137 |
| pyrrhotite | natural pyrite was calcined at a temperature of 600 °C for 1h | 138 |
| pyrrhotite (Fe7S8) | reaction between iron chloride (FeCl3) and thiourea | 139 |
| sulfide-modified Fe | dithionite was added to sodium borohydride solution. Nano-SiO2 was added into the solution. After that, the mixture was titrated into a FeCl3 solution | 140 |
| sulfide-modified ZVI | sodium borohydride and dithionite were added to FeCl3 solution in a dropwise manner | 141 |
| sulfur modified Fe | iron and sulfur were mixed in an exothermic reaction | 142 |

Fig. 6 Fe-S system phase diagram showing iron sulfide transition from FeS to FeS2 at different temperatures (25-1200°C) (reproduced from Wang and Salveson (2005) 23 with permission)

## Solvothermal and hydrothermal methods

Solvothermal and hydrothermal methods are commonly used to fabricate various types of engineered NPs and can be applied to produce high quality SINPs.  The most common reducing agents for solvothermal methods include dithionite and borohydride.  Dithionite is widely used in research and industry because it is a relatively low-cost substance that decomposes in aqueous solution to form hydrogen sulfide (H2S), which in the presence of dissolved Fe2+ leads to the precipitation of iron sulfide SINPs 143, 144.  However, unintended precipitation products of solvothermal methods may cause impurities that need mitigation.  A slight excess of sulfide can help prevent soluble Fe2+ from precipitating as iron hydroxide in mackinawite SINP synthesis 32.

### Pyrite SINPs

Pyrite SINPs of various morphologies can be formed by solvothermal and hydrothermal methods.  For example, single-phase pyrite SINPs of crystallographic purity and good size uniformity (2~5 nm) can be formed using FeCl2·4H2O (1.3 mmol) in dimethyl sulfoxide containing thioglycolic acid, with Na2S2O3·5H2O added under continued stirring and N2 purging.  FeS2 NPs form if the temperature is raised to boiling point, which can then be further crystallized under reflux 55.  This method can be modified to produce pyrite SINPs of different morphologies.  Nanowires and nanosheets can also be synthesized using the same precursors with only a slight modification of the method 145.

The synthesis of FeS2 SINPs with nanorod type morphologies can be achieved using  a solvothermal process involving FeS2 in ethylenediamine to produce SINPs of 20~50 nm in diameter and up to 1000 nm in length 146.  The precise morphology depends on the type of solvent used (Fig. 7).  Colloidal pyrite SINPs can be produced by injecting sulfur-diphenyl ether solution into FeCl2-octadecylamine solution at 220 °C 54.  Pyrite SINPs have also been synthesized using iron(II) chloride tetrahydrate (FeCl2-4H2O) and sodium thiosulfate pentahydrate (Na2S2O3-5H2O) as precursors 61.

Fig. 7 Different FeS2 SINP morphologies resulting from the use of different solvothermal solvents: (a) ethylenediamine solvent (b) benzene solvent (reproduced from Xuefeng et al., (2001) 146 with permission)

In single-stage hydrothermal synthesis using a mixture of FeSO4 with Na2S2O3 and elemental S in water at 90–280 °C, lengthy reaction times (24 h) favor the formation of pyrite crystals 147.  The resulting SINPs have an average particle size of ~500 nm, and are AB2 cubic structured (space group Pa3, lattice constant a=5.4151 Å, and Wyckoff parameter u=0.3868).  SEM images (Fig. 8) illustrate a well-crystallized polycrystalline pyrite form.

Fig. 8 Scanning electron microscopy (SEM) images of FeS2 SINPS prepared from a mixture of FeSO4 with Na2S2O3 and elemental S in water for 24 h at 200 °C for 24 h (reproduced from Wu et al., (2004) 147 with permission)

The possible mechanism for the formation of pyrite SINPs from Na2S2O3, elemental S, and FeSO4 was reported as follows: 147

Na2S2O3+H2O=H2S↑+Na2SO4

As H2S is saturated in aqueous solution, the following equilibria exist:

H2S⇄H++HS−

HS−⇄H+S2-

The added elemental S is deoxidized by hydrosulphuric acid, which releases H2S:

S+2H++2e⇄H2S↑

FeS is formed as the added FeSO4 releases Fe2+ ions, and the ionic products of Fe2+ and S2- exceed the solubility product of FeS.  The solubility of H2S is low, so it exists mostly as gaseous phase, driving the following pyrite forming reaction:

H2S+FeS=FeS2+H2

There are various factors that influence the size and morphology of pyrite SINPs produced by hydrothermal methods using different S sources 98.  Synthesis procedures using elemental S proceed via polysulfide, produce mainly octahedral pyrite particles, whereas synthesis using H2S proceed via FeS and H2S, produce much smaller NPs with diverse morphologies, including cubes and framboids.  The synthesis of high quality phase-pure and single crystalline pyrite nanoparticles via the hydrothermal route has been accomplished wherein the reaction time and S:Fe molar ratio play important roles in the quality and morphology of FeS2 nanocrystals produced. A high sulfur to iron molar ratio and longer reaction times are beneficial for this purpose 148.

### FeS SINPs

Synthesis of (approximate) iron sulfide (FeS) NPs can easily be achieved by wet chemical reduction and the formed FeS SINPs separated by filtration.  A tentative chemical reaction for such a process is as follows 149:

2Fe(NO3)3·9H2O + 3C4H4Na2O6·2H2O + 2Na2S2O3·5H2O → FeS + 6NaNO3 + 2Na2SO3 + C4H4Na2O6(aq)

The synthesis of FeS SINPs with needle-like morphology can be achieved via the Schlenk technique under a N2 atmosphere 130 and autoclaving the solution at 150 °C for 12 h followed by centrifugation. Colloidal nanosheets of mackinawite (FeS) can also be synthesized by co-precipitating an amorphous Fe-S precursor, which is first formed by rapid injection of Na2S into a FeCl2 solution, followed by centrifugation, sonication of the precipitate in ethylene glycol, and heating in an autoclave to 200 °C.  The resulting product has lattice constants of a = 3.674(3) Å and c = 5.0354(3) Å, with the nanosheets irregularly faceted of length 100 nm to > 1 mm and ~30 nm thicknesses with the surface normal oriented along the [0 0 1] direction 24. Variations of the synthesis procedure can also produce Fe/FeS SINPs of 20~30 nm size and high specific surface areas of 30~40 m2/g 143.

### Other SINP types

The synthesis of pyrrhotite (Fe7S8) SINPs (~30 nm) can be accomplished by mixing iron(III) chloride hexa-hydrate and thiourea in a mixture of ethylene glycol H2O, and autoclaving the mixture at high temperature 139.  Similarly, both nanowires and nanosheets of pyrrhotite can be produced by varying the synthesis conditions and processing of the resultant precipitate 150, 151.  A variety of synthesis methods have also been used to generate and stabilize greigite nanocrystals 152, 153, which display excellent sorption capacity and separation properties. Bimetallic FeMoS nanoparticles can be synthesized via thermal decomposition of iron hteteropolymolybdates and Fe7O8 SINPs, with various morphological properties (i.e., spherical, rods, or plates), can be produced by varying the growth temperature and precursor concentration used 154.

Greigite, pyyrrhotite, and mixed phase SINPs have also been synthesized using symmetrical- and unsymmetrical-dia-lkyldithiocarbamatoiron(III) complexes 36.  Aligned cubic phase FeS2-x nanowires can be formed using iron nitrate (Fe(NO3)3.9H2O) and sodium sulfide (Na2S) 155, and different nano-crystalline iron sulfides can be produced by reacting FeSO4.7H2O with Na2S3 in toluene simply by changing the reaction temperature and time 156. High-purity spinel Fe3S4 SINPs can be synthesized by dissolving L-cysteine in water and then adding FeSO4 157.

## Mechanical milling and alloying

Physical formation of nano-sized particulate powder by high-energy milling is referred to as mechanical milling, whereas the milling of a mixture of different metals and compounds has been termed mechanical alloying 158.  In mechanical milling, mechanical energy is applied, typically at room temperature, to stimulate chemical reactions and phase transformations, which would otherwise only occur at elevated temperatures 159.  Ball milling induces multiple forces, including shear stress, triaxial stress, and hydrostatic stresses 158, and results in processes such as high-speed plastic deformation, cold welding, thermal shock, and complete mixing 160.

Mechanical milling can be used to produce pyrite and troilite SINPs 131, 160, 161, and elemental iron has been used as a reducing reagent for high-energy alloying to synthesize Me/FeS (Me=Cu, Pb, Sb) nanocomposites 162.

## Biosynthesis

Biosynthesis has also been used to produce SINPs.  An advantage of this approach is that it can be conducted at ambient temperature, pH, and pressure, without being energy intensive or requiring specialty reagents 163.  A variety of biosynthetic approaches have been employed, including direct processes such as biologically induced mineralization, or biologically controlled mineralization.  In the former, NPs result from metabolic processes, e.g., as solid substrates attached to bacteria, or by interaction with bacterial cell walls/membranes (Fig. 9).  For the latter process, nucleation and growth of NPs occurs within microbial cells.  The resultant nanoparticles tend to be formed of well-defined crystals with narrow particle-size distributions 164.  Engineered NPs can also be produced by indirect biosynthesis, via redox reactions that occur due to the presence of microbes.

Fig. 9 TEM images showing the biosynthesis of FeS nanoparticles by S. oneidensis (A) SINPs on the cell surface; and (B) SINPs suspended in the medium (electron diffraction pattern shown inset) (reproduced from Xiao et al., (2016) 127 with permission)

Dissimilatory metal-reducing bacteria, such as Shewanella, are of interest because they reduce Fe(III) to Fe(II) species 127, 165, which can then precipitate with sulfide to form biogenic SINPs.  Actinobacter sp. can also be tuned for extracellular synthesis of SINPs, when reacted with aqueous solutions of ferric chloride-ferrous sulfate 163. A concentrated bacteria (S. putrefaciens CN32) culture can be used for the biosynthesis of FeS SINPs 165.

Shewanella species can also reduce thiosulfate 127 with S. oneidensis MR-1 and gene-modified strains having been used to produce FeS SINPs.  The biosynthesis of single domain greigite SINPs by MTB has also been explored 166, 167, but greigite SINP formation occurs under anaerobic conditions, and thus requires further downstream processing, which may be too expensive for large-scale SINP synthesis.

## Green and sustainable synthesis methods

Recently, various procedures for green NP synthesis have been advanced.  Compared to conventional synthesis, green and sustainable synthesis seeks either: (i) the use of green materials as synthesis reagents, or (ii) the employment of production methods that consume less energy or natural resources 168.  There are various ways of achieving these aims. For example, using natural plant extracts and microbiological materials as reducing, capping, and stabilizing reagents, or using ultrasound irradiation to reduce energy and reagent requirements.  Such techniques are noted for having lower associated environmental impacts than traditional synthesis techniques 169, 170.

Different biomaterials as stabilizers, including glucose, starch, carboxymethylcellulose (CMC), yeast extract, beef extract, peptone and gelatin, can be used to form stable FeS SINPs 171.  By using thiourea as a sulfide source, FeCl2 as an iron source, and ethylene glycol as a solvent, the synthesis of pyrite SINPs in a one-pot solvothermal synthesis can be achieved without surfactants, at ambient pressure and relatively low temperature. If the temperature of this synthesis reaction is maintained at boiling point (~180 °C) under reflux at atmospheric pressure, pyrite SINPs of ~25 nm will form 172.   For these SINPs, a slight increase of the unit-cell parameter and crystallinity compared to published data for bulk pyrite may result from surface effects.

Another pathway to attain greener and sustainable synthesis of SINPS is by recovering materials from waste streams for reuse.  For example, S species such as sulfite and thiosulfate, or their reduction product H2S, may be harvested from industrial wastewaters.  Recovery of these otherwise wasted chemicals also brings environmental benefits by mitigating a potential source of environmental pollution 173, 174.  For example, Shewanella bacteria have been exploited to reduce thiosulfate in industrial wastewaters in order to fabricate FeS SINPs, thus achieving both pollution control and SINP biosynthesis 127.

Thermal reactions have also been developed to prepare green SINPs without the use of hazardous organic solvents or surfactants.  For example, mixing ferrocene and elemental S (2.325:1 ratio) and annealing them (without a solvent) at 500 °C under an N2 atmosphere generates a FeS2 and carbon nanocomposite product 175.

## Other synthesis methods and enhancements

### Chemical vapor deposition

Chemical vapor deposition (CVD) is a well-established method for the preparation of elemental and compound semiconductors, a method that brings the possibility of constituent flux control, in order to adjust stoichiometry.  CVD is a means to prepare the epitaxial layers on single crystalline substrates, and, in this way, the influence of grain boundaries on photovoltaic (PV) properties can be explored 176. As one example, highly textured Fe(1+x)S (0.1<x<0.2) SINPs with rod-like morphology can be deposited on Si by CVD using iron(III) N,N-diethyldithiocarbamate as a single source precursor. Vacuum evaporation of the precursor, followed by thermal decomposition on a silicon substrate, results in the growth of Fe-rich FeS semiconductors 177.

### Magnetron sputtering and ion sputtering

A variety of SINPs have been prepared by magnetron sputtering and ion sputtering.  For instance, pyrite SINP with aggregate morphologies can be formed at 400 °C by this process using transitional iron sulfides.  Pyrite SINPs formed at 460 °C have more uniform particle size distributions, and the use of longer annealing time forms crystallite SINPs of more distinguishable structure, with the disappearance of obvious aggregation.  The electrical resistivity of pyrite films prepared at both temperatures also increases with increased annealing time 178.

### Ultrasound irradiation (sonication)

Ultrasound irradiation can be exploited to aid the synthesis of SINPs wherein the chemical effects are derived from acoustic cavitation formation, growth, and implosive collapse.  For instance, pyrite SINPs can be formed in this way, with the ensuing SINPs displaying two phases of pyrite (cubic and marcasite), the average SINP size being ~29 nm.  FT-IR and Raman spectra also suggest the presence of Fe=S, Fe-S and S-S functional groups 179.  Mackinawite-like FeS SINPs and Cu doped FeS SINPS can be similarly formed using ultrasound irradiation by adjusting the synthesis conditions and post-synthesis treatment procedures 180.  Pyrite SINPs can also be synthesized with the aid of ultrasound irradiation by one-step sonication and autoclaving 181.

### Plasma processes

The use of non-thermal N2 plasma processes may be an effective approach for the preparation of SINP materials from natural bulk minerals, owing to the sputtering effect.  An example of this method is the adding of crushed pyrite ore (micro-sized) to a glow discharge plasma reactor. The reactor comprises a horizontal borosilicate tube of N2 gas with a high voltage direct current supplied via aluminum bonnets.  The pyrite SINPs fabricated by this method are in the 30-50 nm size range.  The chemical structure of pyrite is not affected by plasma processes, but it should be noted that SINPS formed this way may display irregular rough surfaces 132.

### Subtractive methods

Subtractive methods can be applied for the formation of various SINPs including the synthesis of FeS2 nanotubes from iron oxide nanotubes (produced anodically before sulfurization) with S vapor 182.  Other metal oxides nanotubes and porous structures could potentially be converted to sulfide nanotubes and porous sulfides in the same manner. However, optimization of structure retention and phase purity requires further research.  Additionally, the advantage of sulfurization with elemental S rather than H2S needs further consideration 183.

### Template-directed synthesis

By using a sol–gel method, highly ordered iron pyrite (FeS2) nanowires and nanotube arrays can be fabricated using templates composed of materials such as anodic aluminum oxide (AAO)  49. For this procedure, hydrate ferric nitrate solvents are heated while stirring.  Nano-porous AAO template tubes (200 nm internal diameter) are then added under negative pressure to ensure the tube spaces are filled before annealing to form nanotubes.  If this is repeated three times, nanowires will be formed instead of tubes.  Afterwards, SINPs are formed by further annealing in a sulfurous atmosphere.  Finally, the AAO template is removed using a NaOH solution (Fig. 10).  The resultant SINP nanowires and nanotubes crystal phase is cubic FeS2.  The nanotubes do not display a clear absorption edge, and the FeS2 nanowires have direct optical band gaps of 0.98 and 1.23 eV, respectively, indicating suitability for PV applications.

Fig. 10 Schematic of a possible formation mechanism of FeS2 nanowires and nanotubes by sol–gel and sulfurization (adapted from Li et al., (2014) 49 with permission)

### Polyol-mediated process

Polyol processes exploit high-boiling polyalcohol solvents such as glycerol, diethylene glycol, ethylene glycol, tetraethylene glycol, which also function as mild reducing agents.  This method was originally developed for the synthesis of nanocrystalline late transition elements (e.g., Pd), but it can be adapted for the synthesis of SINPs.

For the production of greigite SINPs by a polypol-mediated method, Fe(COOCH3)2 can be used as a cation source, polyvinylpyrrolidone powder as a capping agent, and thiourea as a S source in a diethylene glycol solvent under an Ar atmosphere.  If the mixture is refluxed under stirring, a black precipitate of polyvinylpyrrolidone powder-coated Fe3S4 SINPs (9-20 nm) form, which can be separated using an external magnetic field.  Of these, the smaller sized SINP particles are nonstoichiometric greigite with cation vacancy, while the larger SINPs consist of stoichiometric greigite.  These SINPs display ferrimagnetic behavior at -195 to 27 °C with a magnetic moment of ≈ 3.5 μB per Fe3S4 unit 29. This method is noted for its low reaction temperature and pressure, making it aligned with green synthesis.

### Carbon supported SINPs

Common to other NPs, SINPs are vulnerable to coalescing into aggregates, owing to their surface energy, Van der Waals forces, magnetic attraction, and other interactions.  Support materials can reduce the tendency of SINP products to agglomerate.  Ideally, the support materials used for environmental applications should: (i) be chemically and physically stable; (ii) show strong surface chemical-physical binding with the SINP; (iii) be of high specific surface area; (iv) show good adsorption capacity for any contaminants of concern, if applicable; (v) be favorable for liquid-solid phase separation, and (vi) be amenable to simple reactor designs with low mass transfer limitations 184.  Suitable solid support materials can also expand the effective pH range 185.

Organic C support matrices can potentially match these requirements. Biochar is a recalcitrant form of C produced by the pyrolysis of biomass 186, which can be used as a support for SINPs. For example, FeS SINPs can attach to biochar surfaces via -OH, C=C, O=C-O, C-O, and Si-O functional groups, providing these SINPs with excellent adsorption and reducing capability. These characteristics make this material suitable for Cr(VI) removal from polluted waters, in one such case, 57% of Cr(VI) removal was attributed to reduction reactions and the remainder attributed to adsorption 121.

# Summary and future research directions

Our understanding of SINP formation in the natural environment has been enhanced by studies of submarine hydrothermal vents, as well as studies of SINPs in the lithosphere, microbial processes, and even in outer space.  Consequently, we are now aware of some of the key role SINPs play in many natural systems, and this is of importance for the development of engineered SINP synthesis procedures.  For example, the use of H2S as a sulfur source with SiO2 allows the synthesis of pyrite particles that are morphologically similar to those observed at hydrothermal vents, 98 exemplifying the potential for nature-based solutions.  Moreover, there has been increasing use of nature-based biosynthesis approaches for the fabrication of engineered NPs.

With increasing interest in greener and sustainable practices among the research community 187, 188, traditional engineered NP synthesis techniques are becoming more of a concern due to their high energy and resource demand, and the use of potentially hazardous or environmentally harmful reagents 189, 190.  For example, conventional solvothermal synthesis often uses toxic organic solvents.  To circumvent this, researchers are developing facile one-step methods that use common laboratory regents.  Reducing the environmental impacts of SINP synthesis is particularly significant when the product is used for environmental remediation purposes where the main goal is to protect human health and the environment.  Previously, researchers have concentrated on maximizing efficacy and achieving remediation goals, but more holistic approaches in the development of new greener remediation materials are needed for a sustainable future191-194.

Research output pertaining to SINP formation has increased dramatically in recent years, but further opportunities need to be identified and there are still challenges to be faced. There are exciting new directions for research on SINPs, including studies involving regeneration or upscaling synthetic protocols to aid the commercialization of SINPs, however, improved green synthesis approaches must be first developed to alleviate concerns regarding some of the more toxic synthesis process presently used.

AUTHOR INFORMATION

Corresponding Authors

* Corresponding authors (houdeyi@tsinghua.edu.cn; varma.rajender@epa.gov)

Notes

The authors declare no competing financial interest.

Biographies

Dr. David O’Connor

Dr. O’Connor conducts high-impact scientific research on sustainable land management. He is a graduate of Cambridge University where he also worked as a postdoctoral researcher after being awarded an EPSRC doctoral prize. Since 2016 he has worked at Tsinghua University, Beijing. His research principle is that sustainable land management is fundamental for achieving the sustainable development goals and meeting the food demand of the world’s growing population. David’s research has led to the publication of 48 SCI articles in journals including Nature, Science, Nature Sustainability, Nature Reviews: Earth & Environment. He is currently serving as an Associate Editor for Soil Use and Management, and as an editorial board member for the Journal of Hazardous Materials and Science of the Total Environment.

Dr. Deyi Hou

Dr. Hou is an Associate Professor at the School of Environment of Tsinghua University in Beijing, China. Deyi’s research interest includes sustainability of soil use and management, regional to global sources and distribution of heavy metal pollution, contaminant transport and fate in porous media, green and innovative remediation materials and technologies, etc. Deyi received his B.E. from Tsinghua University, M.S. from Stanford University, and Ph.D. from University of Cambridge. He has published over 100 papers on international journals including Nature, Science, Nature Climate Change, Nature Sustainability, etc. He is currently serving as an Editor-in-Chief for Soil Use and Management, and Associate Editor for Science of the Total Environment. He also serves as an editorial board member for Critical Reviews in Environmental Science and Technology, Environmental Pollution, and Remediation Journal. He has also served as co-chair, session chair, and scientific committee members for tens of international conferences.

Prof. Qingsong Liu

Prof. Liu is a Chair professor in Department of Ocean Science and Engineering, Southern University of Science and Technology. His scientific interests focus on marine magnetism. He and his team investigate variations of the Earth’s magnetic field recorded by different natural media on different time scales. In addition, they aim to construct fluctuations of global Aeolian dust and its linkage to oceanic productivity and global CO2 cycle. Dr. Liu has coauthored over 180 peer-reviewed scientific publications.

Prof. Martin Palmer

Prof. Palmer is an ISI Highly Cited Scientist and a Fellow of the Geochemical Society and the European Society of Geochemistry.  He received a BSc in Chemistry from the University of East Anglia (UK) in 1980 and a PhD from the University of Leeds (UK) in 1984.  He is currently a professor in the School of Ocean and Earth Science at the University of Southampton.  He has published nearly 200 papers in the peer-reviewed literature on many aspects of geochemistry.  These publications include studies of nanoparticles in marine sediments, the chemistry nanoparticles released from prosthetic joint implants and the source and impact of nanoparticles in atmospheric pollution.

Prof. Rajender Varma

Prof. Varma (H-Index 111, Highly Cited Researchers 2016,18,19; Publons Awardee 2018, 2019) was born in India (Ph.D., Delhi University 1976). After postdoctoral research at Robert Robinson Laboratories, Liverpool, U.K., he was a faculty member at Baylor College of Medicine and Sam Houston State University prior to joining the Sustainable Technology Division at the U.S. Environmental Protection Agency in 1999. He has a visiting scientist’s position at Regional Centre of Advanced Technologies and Materials, Palacky University at Olomouc, Czech Republic. He has over 45 years of research experience in management of multidisciplinary technical programs ranging from natural products chemistry to development of more environmentally friendly synthetic methods using microwaves, ultrasound, etc. Lately, he is focused on greener approaches to assembly of nanomaterials and sustainable applications of magnetically retrievable nanocatalysts in benign media. He is a member of the editorial advisory board of several international journals, has published over 615 papers, and has been awarded 17 U.S. Patents, 6 books, 26 book chapters, and 3 encyclopedia contributions with 43,200 citations.

Author Contributions

The manuscript was written through contributions of all authors. All authors have given approval to the final version of the manuscript.

Acknowledgements

This work was supported by National Key Research and Development Program of China (Grant No. 2018YFC1801300), and the National Water Pollution Control and Treatment Science and Technology Major Project (No. 2018ZX07109-003).

References

1.	ISO, ISO/TS 80004-2: 2015. Nanotechnologies-Vocabulary-Part 2: Nano-objects. International Organization for Standardization: Geneva, Switzerland, 2015;

2.	Cao, G., Nanostructures and nanomaterials: synthesis, properties and applications. World scientific: Singapore, 2004.

3.	Kelly, K. L.;  Coronado, E.;  Zhao, L. L.; Schatz, G. C., The Optical Properties of Metal Nanoparticles:  The Influence of Size, Shape, and Dielectric Environment. The Journal of Physical Chemistry B 2003, 107 (3), 668-677, 10.1021/jp026731y

4.	Daniel, M. C.; Astruc, D., Gold nanoparticles: assembly, supramolecular chemistry, quantum-size-related properties, and applications toward biology, catalysis, and nanotechnology. Chem Rev 2004, 104 (1), 293-346, 10.1021/cr030698+

5.	Burda, C.;  Chen, X.;  Narayanan, R.; El-Sayed, M. A., Chemistry and properties of nanocrystals of different shapes. Chem Rev 2005, 105 (4), 1025-102, 10.1021/cr030063a

6.	Duan, J.;  Ji, H.;  Zhao, X.;  Tian, S.;  Liu, X.;  Liu, W.; Zhao, D., Immobilization of U(VI) by stabilized iron sulfide nanoparticles: Water chemistry effects, mechanisms, and long-term stability. Chemical Engineering Journal 2020, 393, 124692, 10.1016/j.cej.2020.124692

7.	Wang, M.;  Li, Y.;  Zhao, D.;  Zhuang, L.;  Yang, G.; Gong, Y., Immobilization of mercury by iron sulfide nanoparticles alters mercury speciation and microbial methylation in contaminated groundwater. Chemical Engineering Journal 2020, 381, 122664, 10.1016/j.cej.2019.122664

8.	Lozano, J. G.;  Dillon, F.;  Naylor, A. J.;  Lee, L. Y.;  Lippard, C.;  Johnstone, D.;  Bruce, P. G.; Grobert, N., Single source precursor route to iron sulfide nanomaterials for energy storage. Chemical Physics Letters 2020, 739, 136993, 10.1016/j.cplett.2019.136993

9.	Wu, H.;  Liu, J.;  Liang, H.; Zang, D., Sandwich-like Fe3O4/Fe3S4 composites for electromagnetic wave absorption. Chemical Engineering Journal 2020, 393, 124743, 10.1016/j.cej.2020.124743

10.	Rana, A.;  Yadav, K.; Jagadevan, S., A comprehensive review on green synthesis of nature-inspired metal nanoparticles: Mechanism, application and toxicity. Journal of Cleaner Production 2020, 272, 122880, 10.1016/j.jclepro.2020.122880

11.	Sharma, V. K.;  Filip, J.;  Zboril, R.; Varma, R. S., Natural inorganic nanoparticles--formation, fate, and toxicity in the environment. Chem Soc Rev 2015, 44 (23), 8410-23, 10.1039/c5cs00236b

12.	Hou, D.;  O’Connor, D.;  Igalavithana, A. D.;  Alessi, D. S.;  Luo, J.;  Tsang, D. C. W.;  Sparks, D. L.;  Yamauchi, Y.;  Rinklebe, J.; Ok, Y. S., Metal contamination and bioremediation of agricultural soils for food safety and sustainability. Nature Reviews Earth & Environment 2020, 1 (7), 366-381, 10.1038/s43017-020-0061-y

13.	Trogadas, P.; Coppens, M.-O., Nature-Inspired Chemical Engineering. In Sustainable Nanoscale Engineering, Szekely, G.; Livingston, A., Eds. Elsevier: 2020; pp 19-31.

14.	Kou, J.;  Lu, C.;  Wang, J.;  Chen, Y.;  Xu, Z.; Varma, R. S., Selectivity Enhancement in Heterogeneous Photocatalytic Transformations. Chem Rev 2017, 117 (3), 1445-1514, 10.1021/acs.chemrev.6b00396

15.	Song, Y.;  Kirkwood, N.;  Maksimovic, C.;  Zheng, X.;  O'Connor, D.;  Jin, Y.; Hou, D., Nature based solutions for contaminated land remediation and brownfield redevelopment in cities: A review. Sci Total Environ 2019, 663, 568-579, 10.1016/j.scitotenv.2019.01.347

16.	Chandrawat, G. S.;  Tripathi, J.;  Sharma, A.;  Singh, J.;  Tripathi, S.; Chouhan, J., Study of Structural and Optical Properties of FeS2 Nanoparticles Prepared by Polyol Method. Journal of Nano- and Electronic Physics 2020, 12 (2), 02016-1-02016-3, 10.21272/jnep.12(2).02016

17.	Guan, G.;  Li, B.;  Zhang, W.;  Cui, Z.;  He, S. A.;  Zou, R.;  Lu, X.; Hu, J., High-efficiency and safe sulfur-doped iron oxides for magnetic resonance imaging-guided photothermal/magnetic hyperthermia therapy. Dalton Trans 2020, 49 (17), 5493-5502, 10.1039/d0dt00297f

18.	Shi, Z.; Jayatissa, A. H., Preparation and characterization of cobalt-doped iron pyrite (FeS2) thin films. Progress in Natural Science: Materials International 2020, 30 (3), 352-359, 10.1016/j.pnsc.2020.03.002

19.	Rickard, D.; Luther, G. W., 3rd, Chemistry of iron sulfides. Chem Rev 2007, 107 (2), 514-62, 10.1021/cr0503658

20.	Posfai, M.;  Buseck, P. R.;  Bazylinski, D. A.; Frankel, R. B., Iron sulfides from magnetotactic bacteria; structure, composition, and phase transitions. American Mineralogist 1998, 83 (11-12 Part 2), 1469-1481, 10.2138/am-1998-11-1235

21.	Taylor, L.; Finger, L., Structural refinement and composition of mackinawite. Carnegie Institute of Washington Geophysical Laboratory Annual Report 1970, 69, 318-322,

22.	Akhtar, M.;  Malik, M. A.;  Tuna, F.; O'Brien, P., The synthesis of iron sulfide nanocrystals from tris(O-alkylxanthato)iron(iii) complexes. Journal of Materials Chemistry A 2013, 1 (31), 8766-8774, 10.1039/c3ta12178j

23.	Wang, H.; Salveson, I., A review on the mineral chemistry of the non-stoichiometric iron sulphide, Fe1− x S (0≤ x≤ 0.125): polymorphs, phase relations and transitions, electronic and magnetic structures. Phase Transitions 2005, 78 (7-8), 547-567, 10.1080/01411590500185542

24.	Vaughan, D. J., Mineral chemistry of metal sulfides. Cambridge Earth Sci. Ser., Cambridge 1978, 493,

25.	Dekkers, M. J., Magnetic properties of natural pyrrhotite. II. High- and low-temperature behaviour of Jrs and TRM as function of grain size. Physics of the Earth and Planetary Interiors 1989, 57 (3-4), 266-283, 10.1016/0031-9201(89)90116-7

26.	Zhang, B.;  de Wijs, G. A.; de Groot, R. A., Switchable Fermi surface sheets in greigite. Physical Review B 2012, 86 (2), 020406, 10.1103/PhysRevB.86.020406

27.	Skinner, B. J.;  Erd, R. C.; Grimaldi, F. S., Greigite, the thio-spinel of iron; a new mineral. American Mineralogist: Journal of Earth and Planetary Materials 1964, 49 (5-6), 543-555,

28.	Uda, M., On the synthesis of greigite. Am. Mineral. 1965, 50, 1487-1489,

29.	Lyubutin, I. S.;  Starchikov, S. S.;  Lin, C.-R.;  Lu, S.-Z.;  Shaikh, M. O.;  Funtov, K. O.;  Dmitrieva, T. V.;  Ovchinnikov, S. G.;  Edelman, I. S.; Ivantsov, R., Magnetic, structural, and electronic properties of iron sulfide Fe3S4 nanoparticles synthesized by the polyol mediated process. Journal of Nanoparticle Research 2013, 15 (1), 10.1007/s11051-012-1397-0

30.	Beal, J. H. L.;  Prabakar, S.;  Gaston, N.;  Teh, G. B.;  Etchegoin, P. G.;  Williams, G.; Tilley, R. D., Synthesis and Comparison of the Magnetic Properties of Iron Sulfide Spinel and Iron Oxide Spinel Nanocrystals. Chemistry of Materials 2011, 23 (10), 2514-2517, 10.1021/cm2002868

31.	Taylor, P., The stereochemistry of iron sulfides—a structural rationale for the crystallization of some metastable phases from aqueous solution. American Mineralogist 1980, 65 (9-10), 1026-1030,

32.	Jeong, H. Y.;  Lee, J. H.; Hayes, K. F., Characterization of synthetic nanocrystalline mackinawite: crystal structure, particle size, and specific surface area. Geochim Cosmochim Acta 2008, 72 (2), 493-505, 10.1016/j.gca.2007.11.008

33.	Horng, C. S.; Roberts, A. P., The low‐temperature Besnus magnetic transition: Signals due to monoclinic and hexagonal pyrrhotite. Geochemistry, Geophysics, Geosystems 2018, 19 (9), 3364-3375, 10.1002/2017JB015262.

34.	Horng, C.-S.; Roberts, A. P., Authigenic or detrital origin of pyrrhotite in sediments?: Resolving a paleomagnetic conundrum. Earth and Planetary Science Letters 2006, 241 (3-4), 750-762, 10.1016/j.epsl.2005.11.008

35.	Harada, T., Transport Properties of Iron Dichalcogenides FeX2(X=S, Se and Te). Journal of the Physical Society of Japan 1998, 67 (4), 1352-1358, 10.1143/jpsj.67.1352

36.	Akhtar, M.;  Akhter, J.;  Malik, M. A.;  O'Brien, P.;  Tuna, F.;  Raftery, J.; Helliwell, M., Deposition of iron sulfide nanocrystals from single source precursors. Journal of Materials Chemistry 2011, 21 (26), 9737-9745, 10.1039/c1jm10703h

37.	Nakazawa, H.;  Morimoto, N.; Watanabe, E., Direct observation of metal vacancies by high-resolution electron microscopy. Part I: 4 C type pyrrhotite (Fe7S8). American Mineralogist: Journal of Earth and Planetary Materials 1975, 60 (5-6_Part_1), 359-366,

38.	Li, F.; Franzen, H. F., Ordering, incommensuration, and phase transitions in pyrrhotite: Part II: a high-temperature X-ray powder diffraction and thermomagnetic study. Journal of Solid State Chemistry 1996, 126 (1), 108-120, 10.1006/jssc.1996.0318

39.	Yue, G. H.;  Yan, P. X.;  Fan, X. Y.;  Wang, M. X.;  Qu, D. M.;  Yan, D.; Liu, J. Z., Characterization of the single crystalline iron sulfide nanowire array synthesis by pulsed electrodeposition. Journal of Applied Physics 2006, 100 (12), 4, 10.1063/1.2403243

40.	Abdelhady, A. L.;  Malik, M. A.;  O’Brien, P.; Tuna, F., Nickel and Iron Sulfide Nanoparticles from Thiobiurets. The Journal of Physical Chemistry C 2012, 116 (3), 2253-2259, 10.1021/jp2078659

41.	Dekkers, M. J.;  Passier, H. F.; Schoonen, M. A. A., Magnetic properties of hydrothermally synthesized greigite (Fe3S4)--II. High- and low-temperature characteristics. Geophysical Journal International 2000, 141 (3), 809-819, 10.1046/j.1365-246x.2000.00129.x

42.	Kasama, T.;  Pósfai, M.;  Chong, R. K.;  Finlayson, A. P.;  Buseck, P. R.;  Frankel, R. B.; Dunin-Borkowski, R. E., Magnetic properties, microstructure, composition, and morphology of greigite nanocrystals in magnetotactic bacteria from electron holography and tomography. American Mineralogist 2006, 91 (8-9), 1216-1229, 10.2138/am.2006.2227

43.	Roberts, A. P.;  Chang, L.;  Rowan, C. J.;  Horng, C.-S.; Florindo, F., Magnetic properties of sedimentary greigite (Fe3S4): An update. Reviews of Geophysics 2011, 49 (1), 10.1029/2010rg000336

44.	Li, L.;  Caban-Acevedo, M.;  Girard, S. N.; Jin, S., High-purity iron pyrite (FeS2) nanowires as high-capacity nanostructured cathodes for lithium-ion batteries. Nanoscale 2014, 6 (4), 2112-8, 10.1039/c3nr05851d

45.	Chang, L.;  Rainford, B. D.;  Stewart, J. R.;  Ritter, C.;  Roberts, A. P.;  Tang, Y.; Chen, Q., Magnetic structure of greigite (Fe3S4) probed by neutron powder diffraction and polarized neutron diffraction. Journal of Geophysical Research 2009, 114 (B7), 10.1029/2008jb006260

46.	Chang, L.;  Roberts, A. P.;  Rowan, C. J.;  Tang, Y.;  Pruner, P.;  Chen, Q.; Horng, C.-S., Low-temperature magnetic properties of greigite (Fe3S4). Geochemistry, Geophysics, Geosystems 2009, 10 (1), n/a-n/a, 10.1029/2008gc002276

47.	Chang, L.;  Roberts, A. P.;  Tang, Y.;  Rainford, B. D.;  Muxworthy, A. R.; Chen, Q., Fundamental magnetic parameters from pure synthetic greigite (Fe3S4). Journal of Geophysical Research 2008, 113 (B6), 10.1029/2007jb005502

48.	Chang, L.;  Roberts, A. P.;  Muxworthy, A. R.;  Tang, Y.;  Chen, Q.;  Rowan, C. J.;  Liu, Q.; Pruner, P., Magnetic characteristics of synthetic pseudo-single-domain and multi-domain greigite (Fe3S4). Geophysical Research Letters 2007, 34 (24), 10.1029/2007gl032114

49.	Li, Y.;  Han, Z.;  Jiang, L.;  Su, Z.;  Liu, F.;  Lai, Y.; Liu, Y., Template-directed synthesis of ordered iron pyrite (FeS2) nanowires and nanotubes arrays. Journal of Sol-Gel Science and Technology 2014, 72 (1), 100-105, 10.1007/s10971-014-3425-2

50.	Jia, X.;  Chen, Z.;  Cui, X.;  Peng, Y.;  Wang, X.;  Wang, G.;  Wei, F.; Lu, Y., Building robust architectures of carbon and metal oxide nanocrystals toward high-performance anodes for lithium-ion batteries. ACS Nano 2012, 6 (11), 9911-9, 10.1021/nn303478e

51.	Chang, Y. S.;  Savitha, S.;  Sadhasivam, S.;  Hsu, C. K.; Lin, F. H., Fabrication, characterization, and application of greigite nanoparticles for cancer hyperthermia. J Colloid Interface Sci 2011, 363 (1), 314-9, 10.1016/j.jcis.2010.06.069

52.	Li, G.;  Zhang, B.;  Yu, F.;  Novakova, A. A.;  Krivenkov, M. S.;  Kiseleva, T. Y.;  Chang, L.;  Rao, J.;  Polyakov, A. O.; Blake, G. R., High-purity Fe3S4 greigite microcrystals for magnetic and electrochemical performance. Chemistry of Materials 2014, 26 (20), 5821-5829, 10.1021/cm501493m

53.	Ding, C.;  Yan, Y.;  Xiang, D.;  Zhang, C.; Xian, Y., Magnetic Fe3S4 nanoparticles with peroxidase-like activity, and their use in a photometric enzymatic glucose assay. Microchimica Acta 2015, 183 (2), 625-631, 10.1007/s00604-015-1690-6

54.	Puthussery, J.;  Seefeld, S.;  Berry, N.;  Gibbs, M.; Law, M., Colloidal iron pyrite (FeS2) nanocrystal inks for thin-film photovoltaics. Journal of the American Chemical Society 2010, 133 (4), 716-719, 10.1021/ja1096368

55.	Bai, Y.;  Yeom, J.;  Yang, M.;  Cha, S.-H.;  Sun, K.; Kotov, N. A., Universal Synthesis of Single-Phase Pyrite FeS2 Nanoparticles, Nanowires, and Nanosheets. The Journal of Physical Chemistry C 2013, 117 (6), 2567-2573, 10.1021/jp3111106

56.	Ennaoui, A.;  Fiechter, S.;  Jaegermann, W.; Tributsch, H., Photoelectrochemistry of highly quantum efficient single‐crystalline n‐FeS2 (Pyrite). Journal of the Electrochemical Society 1986, 133 (1), 97-106,

57.	Antonucci, V.;  Giordano, N.;  Antonucci, P.;  Russo, U.;  Cocke, D.; Crea, F., Photoactive screen-printed pyrite anodes for electrochemical photovoltaic cells. Solar cells 1991, 31 (2), 119-141, 10.1016/0379-6787(91)90016-I

58.	Ennaoui, A.;  Fiechter, S.;  Tributsch, H.;  Giersig, M.;  Vogel, R.; Weller, H., Photoelectrochemical energy conversion obtained with ultrathin organo‐metallic‐chemical‐vapor‐deposition layer of FeS2 (pyrite) on TiO2. Journal of the Electrochemical Society 1992, 139 (9), 2514-2518,

59.	Steinhagen, C.;  Harvey, T. B.;  Stolle, C. J.;  Harris, J.; Korgel, B. A., Pyrite Nanocrystal Solar Cells: Promising, or Fool's Gold? J Phys Chem Lett 2012, 3 (17), 2352-6, 10.1021/jz301023c

60.	Kinner, T.;  Bhandari, K. P.;  Bastola, E.;  Monahan, B. M.;  Haugen, N. O.;  Roland, P. J.;  Bigioni, T. P.; Ellingson, R. J., Majority Carrier Type Control of Cobalt Iron Sulfide (CoxFe1–xS2) Pyrite Nanocrystals. The Journal of Physical Chemistry C 2016, 120 (10), 5706-5713, 10.1021/acs.jpcc.5b11204

61.	Kaur, G.;  Singh, B.;  Singh, P.;  Kaur, M.;  Buttar, K. K.;  Singh, K.;  Thakur, A.;  Bala, R.;  Kumar, M.; Kumar, A., Preferentially grown nanostructured iron disulfide (FeS2) for removal of industrial pollutants. RSC Advances 2016, 6 (101), 99120-99128, 10.1039/c6ra18838a

62.	Nakamura, S.; Yamamoto, A., Electrodeposition of pyrite (FeS2) thin films for photovoltaic cells. Solar Energy Materials and Solar Cells 2001, 65 (1-4), 79-85, 10.1016/S0927-0248(00)00080-5

63.	Takahashi, N.;  Nakatani, Y.;  Yatomi, T.; Nakamura, T., Growth of single-crystal pyrite films by atmospheric pressure chemical vapor deposition. Chemistry of materials 2003, 15 (9), 1763-1765, 10.1021/cm0210243

64.	Deditius, A. P.;  Utsunomiya, S.;  Renock, D.;  Ewing, R. C.;  Ramana, C. V.;  Becker, U.; Kesler, S. E., A proposed new type of arsenian pyrite: Composition, nanostructure and geological significance. Geochimica et Cosmochimica Acta 2008, 72 (12), 2919-2933, 10.1016/j.gca.2008.03.014

65.	Wells, J. D.; Mullens, T. E., Gold-Bearing Arsenian Pyrite Determined by Microprobe Analysis, Cortez and Carlin Gold mines, Nevada. Economic Geology 1973, 68 (2), 187-201, 10.2113/gsecongeo.68.2.187

66.	Kolker, A.;  Haack, S. K.;  Cannon, W. F.;  Westjohn, D.;  Kim, M.-J.;  Nriagu, J.; Woodruff, L., Arsenic in southeastern Michigan. In Arsenic in ground water, Springer: 2003; pp 281-294.

67.	Dai, Z. R.; Bradley, J. P., Iron-nickel sulfides in anhydrous interplanetary dust particles. Geochimica et Cosmochimica Acta 2001, 65 (20), 3601-3612, 10.1016/s0016-7037(01)00692-5

68.	Trepka-Bloch, C., Cyclic ore formation of some volcanogenic massive sulfide deposits in the skellefte district, Sweden. Mineralium Deposita 1985, 20 (1), 23-29, 10.1007/bf00204256

69.	Liang, D.;  Ma, R.;  Jiao, S.;  Pang, G.; Feng, S., A facile synthetic approach for copper iron sulfide nanocrystals with enhanced thermoelectric performance. Nanoscale 2012, 4 (20), 6265-8, 10.1039/c2nr31193c

70.	Chen, Y.;  Xu, S.;  Li, Y.;  Jacob, R. J.;  Kuang, Y.;  Liu, B.;  Wang, Y.;  Pastel, G.;  Salamanca-Riba, L. G.;  Zachariah, M. R.; Hu, L., FeS2

Nanoparticles Embedded in Reduced Graphene Oxide toward Robust, High-Performance Electrocatalysts. Advanced Energy Materials 2017, 7 (19), 10.1002/aenm.201700482

71.	Feng, H.;  Si, P.-Z.;  Xiao, X.-F.;  Jin, C.-H.;  Yu, S.-J.;  Li, Z.-F.; Ge, H.-L., Large scale synthesis of FeS coated Fe nanoparticles as reusable magnetic photocatalysts. Frontiers of Materials Science 2013, 7 (3), 308-311, 10.1007/s11706-013-0213-9

72.	Kim, E. J.;  Kim, J. H.;  Azad, A. M.; Chang, Y. S., Facile Synthesis and Characterization of Fe/FeS Nanoparticles for Environmental Applications. ACS Appl Mater Interfaces 2011, 3 (5), 1457-62, 10.1021/am200016v

73.	Hochella, M. F.;  Spencer, M. G.; Jones, K. L., Nanotechnology: nature's gift or scientists' brainchild? Environmental Science: Nano 2015, 2 (2), 114-119, 10.1039/c4en00145a

74.	Noguchi, T.;  Nakamura, T.;  Kimura, M.;  Zolensky, M. E.;  Tanaka, M.;  Hashimoto, T.;  Konno, M.;  Nakato, A.;  Ogami, T.;  Fujimura, A.;  Abe, M.;  Yada, T.;  Mukai, T.;  Ueno, M.;  Okada, T.;  Shirai, K.;  Ishibashi, Y.; Okazaki, R., Incipient space weathering observed on the surface of Itokawa dust particles. Science 2011, 333 (6046), 1121-5, 10.1126/science.1207794

75.	Benning, L. G.;  Wilkin, R. T.; Barnes, H. L., Reaction pathways in the Fe–S system below 100°C. Chemical Geology 2000, 167 (1-2), 25-51, 10.1016/s0009-2541(99)00198-9

76.	Hunger, S.; Benning, L. G., Greigite: a true intermediate on the polysulfide pathway to pyrite. Geochem Trans 2007, 8, 1, 10.1186/1467-4866-8-1

77.	Maher, B. A.; Thompson, R., Quaternary climates, environments and magnetism. Cambridge University Press: Cambridge, United Kingdom, 1999.

78.	Whitney, J. A.; Stormer Jr, J. C., Igneous sulfides in the Fish Canyon Tuff and the role of sulfur in calc-alkaline magmas. Geology 1983, 11 (2), 99-102,

79.	Peiffer, S.;  Behrends, T.;  Hellige, K.;  Larese-Casanova, P.;  Wan, M.; Pollok, K., Pyrite formation and mineral transformation pathways upon sulfidation of ferric hydroxides depend on mineral type and sulfide concentration. Chemical Geology 2015, 400, 44-55, 10.1016/j.chemgeo.2015.01.023

80.	Berner, R. A., Sedimentary pyrite formation: An update. Geochimica et Cosmochimica Acta 1984, 48 (4), 605-615, 10.1016/0016-7037(84)90089-9

81.	Butler, E. C.; Hayes, K. F., Kinetics of the Transformation of Trichloroethylene and Tetrachloroethylene by Iron Sulfide. Environmental Science & Technology 1999, 33 (12), 2021-2027, 10.1021/es9809455

82.	Dries, J.;  Bastiaens, L.;  Springael, D.;  Diels, L.; Agathos, S. N., Kinetics of trichloroethene (TCE) reduction by zero-valent iron: effect of medium composition. In Groundwater Quality: Natural and Enhanced Restoration of Groundwater Pollution, Thornton, S. F.; Oswald, S. E., Eds. 2002; pp 397-402.

83.	Fan, D.;  Lan, Y.;  Tratnyek, P. G.;  Johnson, R. L.;  Filip, J.;  O'Carroll, D. M.;  Nunez Garcia, A.; Agrawal, A., Sulfidation of Iron-Based Materials: A Review of Processes and Implications for Water Treatment and Remediation. Environ Sci Technol 2017, 51 (22), 13070-13085, 10.1021/acs.est.7b04177

84.	Hellige, K.;  Pollok, K.;  Larese-Casanova, P.;  Behrends, T.; Peiffer, S., Pathways of ferrous iron mineral formation upon sulfidation of lepidocrocite surfaces. Geochimica et Cosmochimica Acta 2012, 81, 69-81, 10.1016/j.gca.2011.12.014

85.	Burton, E. D.;  Bush, R. T.;  Sullivan, L. A.;  Hocking, R. K.;  Mitchell, D. R.;  Johnston, S. G.;  Fitzpatrick, R. W.;  Raven, M.;  McClure, S.; Jang, L. Y., Iron-monosulfide oxidation in natural sediments: resolving microbially mediated S transformations using XANES, electron microscopy, and selective extractions. Environ Sci Technol 2009, 43 (9), 3128-34, 10.1021/es8036548

86.	Picard, A.;  Gartman, A.;  Clarke, D. R.; Girguis, P. R., Sulfate-reducing bacteria influence the nucleation and growth of mackinawite and greigite. Geochimica et Cosmochimica Acta 2018, 220, 367-384, 10.1016/j.gca.2017.10.006

87.	Yabusaki, S.;  Cantrell, K.;  Sass, B.; Steefel, C., Multicomponent reactive transport in an in situ zero-valent iron cell. Environ Sci Technol 2001, 35 (7), 1493-503, 10.1021/es001209f

88.	Savage, K. S.;  Tingle, T. N.;  O’Day, P. A.;  Waychunas, G. A.; Bird, D. K., Arsenic speciation in pyrite and secondary weathering phases, Mother Lode Gold District, Tuolumne County, California. Applied Geochemistry 2000, 15 (8), 1219-1244, 10.1016/s0883-2927(99)00115-8

89.	Richards, J. P.; Kerrich, R., The Porgera gold mine, Papua New Guinea; magmatic hydrothermal to epithermal evolution of an alkalic-type precious metal deposit. Economic Geology 1993, 88 (5), 1017-1052, 10.2113/gsecongeo.88.5.1017

90.	MacLean, P. J.; Fleet, M. E., Detrital pyrite in the Witwatersrand gold fields of South Africa; evidence from truncated growth banding. Economic Geology 1989, 84 (7), 2008-2011, 10.2113/gsecongeo.84.7.2008

91.	Watson, J. H. P.;  Cressey, B. A.;  Roberts, A. P.;  Ellwood, D. C.;  Charnock, J. M.; Soper, A. K., Structural and magnetic studies on heavy-metal-adsorbing iron sulphide nanoparticles produced by sulphate-reducing bacteria. Journal of Magnetism and Magnetic Materials 2000, 214 (1-2), 13-30, 10.1016/s0304-8853(00)00025-1

92.	Friedrich, M. W.; Finster, K. W., Geochemistry. How sulfur beats iron. Science 2014, 344 (6187), 974-5, 10.1126/science.1255442

93.	Kim, Y.;  Lee, Y.; Roh, Y., Microbial Synthesis of Iron Sulfide (FeS) and Iron Carbonate (FeCO3) Nanoparticles. J Nanosci Nanotechnol 2015, 15 (8), 5794-7, 10.1166/jnn.2015.10457

94.	Watson, J. H. P.;  Ellwood, D. C.;  Soper, A. K.; Charnock, J., Nanosized strongly-magnetic bacterially-produced iron sulfide materials. Journal of Magnetism and Magnetic Materials 1999, 203 (1-3), 69-72, 10.1016/s0304-8853(99)00191-2

95.	Bosch, J.;  Lee, K. Y.;  Jordan, G.;  Kim, K. W.; Meckenstock, R. U., Anaerobic, nitrate-dependent oxidation of pyrite nanoparticles by Thiobacillus denitrificans. Environ Sci Technol 2012, 46 (4), 2095-101, 10.1021/es2022329

96.	Elderfield, H.; Schultz, A., Mid-Ocean Ridge Hydrothermal Fluxes and the Chemical Composition of the Ocean. Annual Review of Earth and Planetary Sciences 1996, 24 (1), 191-224, 10.1146/annurev.earth.24.1.191

97.	Yücel, M.;  Gartman, A.;  Chan, C. S.; Luther, G. W., Hydrothermal vents as a kinetically stable source of iron-sulphide-bearing nanoparticles to the ocean. Nature Geoscience 2011, 4 (6), 367-371, 10.1038/ngeo1148

98.	Gartman, A.; Luther, G. W., Comparison of pyrite (FeS2) synthesis mechanisms to reproduce natural FeS2 nanoparticles found at hydrothermal vents. Geochimica et Cosmochimica Acta 2013, 120, 447-458, 10.1016/j.gca.2013.06.016

99.	Mottl, M. J.; McConachy, T. F., Chemical processes in buoyant hydrothermal plumes on the East Pacific Rise near 21°N. Geochimica et Cosmochimica Acta 1990, 54 (7), 1911-1927, 10.1016/0016-7037(90)90261-i

100.	Gartman, A.;  Findlay, A. J.; Luther, G. W., Nanoparticulate pyrite and other nanoparticles are a widespread component of hydrothermal vent black smoker emissions. Chemical Geology 2014, 366, 32-41, 10.1016/j.chemgeo.2013.12.013

101.	Fike, D. A.; Grotzinger, J. P., A paired sulfate–pyrite δ34S approach to understanding the evolution of the Ediacaran–Cambrian sulfur cycle. Geochimica et Cosmochimica Acta 2008, 72 (11), 2636-2648, 10.1016/j.gca.2008.03.021

102.	Strauss, H., Geological evolution from isotope proxy signals — sulfur. Chemical Geology 1999, 161 (1-3), 89-101, 10.1016/s0009-2541(99)00082-0

103.	Goodfellow, W. D.; Jonasson, I. R., Ocean stagnation and ventilation defined by δ34S secular trends in pyrite and barite, Selwyn Basin, Yukon. Geology 1984, 12 (10), 583-586, 10.1130/0091-7613(1984)12<583:Osavdb>2.0.Co;2

104.	Roberts, A. P.;  Reynolds, R. L.;  Verosub, K. L.; Adam, D. P., Environmental magnetic implications of Greigite (Fe3S4) Formation in a 3 m.y. lake sediment record from Butte Valley, northern California. Geophysical Research Letters 1996, 23 (20), 2859-2862, 10.1029/96gl02831

105.	Rowan, C. J.; Roberts, A. P., Magnetite dissolution, diachronous greigite formation, and secondary magnetizations from pyrite oxidation: Unravelling complex magnetizations in Neogene marine sediments from New Zealand. Earth and Planetary Science Letters 2006, 241 (1-2), 119-137, 10.1016/j.epsl.2005.10.017

106.	Snowball, I.; Thompson, R., A stable chemical remanence in Holocene sediments. Journal of Geophysical Research 1990, 95 (B4), 4471-4479, 10.1029/JB095iB04p04471

107.	Duan, Z.;  Liu, Q.;  Gai, C.; Zhao, X., Magnetostratigraphic and environmental implications of greigite (Fe3S4) formation from Hole U1433A of the IODP Expedition 349, South China Sea. Marine Geology 2017, 394, 82-97, 10.1016/j.margeo.2017.02.008

108.	Liu, J.;  Liu, Q.;  Zhang, X.;  Liu, J.;  Wu, Z.;  Mei, X.;  Shi, X.; Zhao, Q., Magnetostratigraphy of a long Quaternary sediment core in the South Yellow Sea. Quaternary Science Reviews 2016, 144, 1-15, 10.1016/j.quascirev.2016.05.025

109.	Morse, J. W.; Luther, G. W., Chemical influences on trace metal-sulfide interactions in anoxic sediments. Geochimica et Cosmochimica Acta 1999, 63 (19-20), 3373-3378, 10.1016/s0016-7037(99)00258-6

110.	Rosenthal, Y.;  Lam, P.;  Boyle, E. A.; Thomson, J., Authigenic cadmium enrichments in suboxic sediments: Precipitation and postdepositional mobility. Earth and Planetary Science Letters 1995, 132 (1-4), 99-111, 10.1016/0012-821x(95)00056-i

111.	Schippers, A.; Jørgensen, B. B., Biogeochemistry of pyrite and iron sulfide oxidation in marine sediments. Geochimica et Cosmochimica Acta 2002, 66 (1), 85-92, 10.1016/s0016-7037(01)00745-1

112.	Rimstidt, J. D.; Vaughan, D. J., Pyrite oxidation: a state-of-the-art assessment of the reaction mechanism. Geochimica et Cosmochimica acta 2003, 67 (5), 873-880, 10.1016/S0016-7037(02)01165-1

113.	Moses, C. O.;  Nordstrom, D. K.;  Herman, J. S.; Mills, A. L., Aqueous pyrite oxidation by dissolved oxygen and by ferric iron. Geochimica et Cosmochimica Acta 1987, 51 (6), 1561-1571, 10.1016/0016-7037(87)90337-1

114.	Singer, P. C.; Stumm, W., Acidic mine drainage: the rate-determining step. Science 1970, 167 (3921), 1121-3, 10.1126/science.167.3921.1121

115.	Schwientek, M.;  Einsiedl, F.;  Stichler, W.;  Stögbauer, A.;  Strauss, H.; Maloszewski, P., Evidence for denitrification regulated by pyrite oxidation in a heterogeneous porous groundwater system. Chemical geology 2008, 255 (1-2), 60-67, 10.1016/j.chemgeo.2008.06.005

116.	Zhang, Z. J.; Chen, X. Y., Magnetic greigite (Fe3S4) nanomaterials: Shape-controlled solvothermal synthesis and their calcination conversion into hematite (α-Fe2O3) nanomaterials. Journal of Alloys and Compounds 2009, 488 (1), 339-345, 10.1016/j.jallcom.2009.08.127

117.	Dwivedi, A. D.;  Dubey, S. P.;  Sillanpää, M.;  Kwon, Y.-N.;  Lee, C.; Varma, R. S., Fate of engineered nanoparticles: Implications in the environment. Coordination Chemistry Reviews 2015, 287, 64-78, 10.1016/j.ccr.2014.12.014

118.	Cheng, D.;  Yuan, S.;  Liao, P.; Zhang, P., Oxidizing Impact Induced by Mackinawite (FeS) Nanoparticles at Oxic Conditions due to Production of Hydroxyl Radicals. Environ Sci Technol 2016, 50 (21), 11646-11653, 10.1021/acs.est.6b02833

119.	Lauretta, D. S.;  Lodders, K.; Fegley, B., Jr., Experimental simulations of sulfide formation in the solar nebula. Science 1997, 277 (5324), 358-60, 10.1126/science.277.5324.358

120.	Zolensky, M. E.; Thomas, K. L., Iron and iron-nickel sulfides in chondritic interplanetary dust particles. Geochimica et Cosmochimica Acta 1995, 59 (22), 4707-4712, 10.1016/0016-7037(95)00329-0

121.	Lyu, H.;  Tang, J.;  Huang, Y.;  Gai, L.;  Zeng, E. Y.;  Liber, K.; Gong, Y., Removal of hexavalent chromium from aqueous solutions by a novel biochar supported nanoscale iron sulfide composite. Chemical Engineering Journal 2017, 322, 516-524, 10.1016/j.cej.2017.04.058

122.	Yang, L.;  Gao, J.;  Liu, Y.;  Zhang, Z.;  Zou, M.;  Liao, Q.; Shang, J., Removal of Methyl Orange from Water Using Sulfur-Modified nZVI Supported on Biochar Composite. Water, Air, & Soil Pollution 2018, 229 (11), 10.1007/s11270-018-3992-x

123.	Gong, Y.;  Liu, Y.;  Xiong, Z.; Zhao, D., Immobilization of mercury by carboxymethyl cellulose stabilized iron sulfide nanoparticles: reaction mechanisms and effects of stabilizer and water chemistry. Environ Sci Technol 2014, 48 (7), 3986-94, 10.1021/es404418a

124.	Esmaili, H.;  Kotobi, A.;  Sheibani, S.; Rashchi, F., Photocatalytic degradation of methylene blue by nanostructured Fe/FeS powder under visible light. International Journal of Minerals, Metallurgy, and Materials 2018, 25 (2), 244-252, 10.1007/s12613-018-1567-x

125.	Wang, X.;  Cai, W.;  Wang, G.;  Wu, Z.; Zhao, H., One-step fabrication of high performance micro/nanostructured Fe3S4-C magnetic adsorbent with easy recovery and regeneration properties. Crystengcomm 2013, 15 (15), 2956-2965, 10.1039/c3ce26856j

126.	Liu, Y.;  Xiao, W.;  Wang, J.;  Mirza, Z. A.; Wang, T., Optimized Synthesis of FeS Nanoparticles with a High Cr(VI) Removal Capability. Journal of Nanomaterials 2016, 10.1155/2016/7817296

127.	Xiao, X.;  Zhu, W.-W.;  Yuan, H.;  Li, W.-W.;  Li, Q.; Yu, H.-Q., Biosynthesis of FeS nanoparticles from contaminant degradation in one single system. Biochemical Engineering Journal 2016, 105, 214-219, 10.1016/j.bej.2015.09.022

128.	Zhang, Q.;  Guo, W.;  Yue, X.;  Liu, Z.; Li, X., Degradation of Rhodamine B Using FeS-Coated Zero-Valent Iron Nanoparticles in the Presence of Dissolved Oxygen. Environmental Progress & Sustainable Energy 2016, 35 (6), 1673-1678, 10.1002/ep.12412

129.	Paknikar, K. M.;  Nagpal, V.;  Pethkar, A. V.; Rajwade, J. M., Degradation of lindane from aqueous solutions using iron sulfide nanoparticles stabilized by biopolymers. Science and Technology of Advanced Materials 2005, 6 (3-4), 370-374, 10.1016/j.stam.2005.02.016

130.	Dutta, A. K.;  Maji, S. K.;  Srivastava, D. N.;  Mondal, A.;  Biswas, P.;  Paul, P.; Adhikary, B., Synthesis of FeS and FeSe nanoparticles from a single source precursor: a study of their photocatalytic activity, peroxidase-like behavior, and electrochemical sensing of H2O2. ACS applied materials & interfaces 2012, 4 (4), 1919-1927, 10.1021/am300408r

131.	Fathinia, S.;  Fathinia, M.;  Rahmani, A. A.; Khataee, A., Preparation of natural pyrite nanoparticles by high energy planetary ball milling as a nanocatalyst for heterogeneous Fenton process. Applied Surface Science 2015, 327, 190-200, 10.1016/j.apsusc.2014.11.157

132.	Khataee, A.;  Gholami, P.; Vahid, B., Heterogeneous sono-Fenton-like process using nanostructured pyrite prepared by Ar glow discharge plasma for treatment of a textile dye. Ultrasonics Sonochemistry 2016, 29, 213-225, 10.1016/j.ultsonch.2015.09.012

133.	Khataee, A.;  Gholami, P.;  Sheydaei, M.;  Khorram, S.; Joo, S. W., Preparation of nanostructured pyrite with N-2 glow discharge plasma and the study of its catalytic performance in the heterogeneous Fenton process. New Journal of Chemistry 2016, 40 (6), 5221-5230, 10.1039/c5nj03594e

134.	Khabbaz, M.; Entezari, M. H., Degradation of Diclofenac by sonosynthesis of pyrite nanoparticles. Journal of Environmental Management 2017, 187, 416-423, 10.1016/j.jenvman.2016.11.005

135.	Gil-Lozano, C.;  Losa-Adams, E.;  F.-Davila, A.; Gago-Duport, L., Pyrite nanoparticles as a Fenton-like reagent for in situ remediation of organic pollutants. Beilstein Journal of Nanotechnology 2014, 5, 855-864, 10.3762/bjnano.5.97

136.	Ito, D.;  Miura, K.;  Ichimura, T.;  Ihara, I.; Watanabe, T., Removal of As, Cd, Hg and Pb ions from solution by adsorption with bacterially-produced magnetic iron sulfide particles using high gradient magnetic separation. Ieee Transactions on Applied Superconductivity 2004, 14 (2), 1551-1553, 10.1109/tasc.2004.830704

137.	Su, Y. M.;  Adeleye, A. S.;  Keller, A. A.;  Huang, Y. X.;  Dai, C. M.;  Zhou, X. F.; Zhang, Y. L., Magnetic sulfide-modified nanoscale zerovalent iron (S-nZVI) for dissolved metal ion removal. Water Research 2015, 74, 47-57, 10.1016/j.watres.2015.02.004

138.	Yang, Y.;  Chen, T.;  Morrison, L.;  Gerrity, S.;  Collins, G.;  Porca, E.;  Li, R.; Zhan, X., Nanostructured pyrrhotite supports autotrophic denitrification for simultaneous nitrogen and phosphorus removal from secondary effluents. Chemical Engineering Journal 2017, 328, 511-518, 10.1016/j.cej.2017.07.061

139.	Cantu, J.;  Gonzalez, L. E.;  Goodship, J.;  Contreras, M.;  Joseph, M.;  Garza, C.;  Eubanks, T. M.; Parsons, J. G., Removal of arsenic from water using synthetic Fe7S8 nanoparticles. Chemical Engineering Journal 2016, 290, 428-437, 10.1016/j.cej.2016.01.053

140.	Su, Y. M.;  Adeleye, A. S.;  Huang, Y. X.;  Zhou, X. F.;  Keller, A. A.; Zhang, Y. L., Direct Synthesis of Novel and Reactive Sulfide-modified Nano Iron through Nanoparticle Seeding for Improved Cadmium-Contaminated Water Treatment. Scientific Reports 2016, 6, 13, 10.1038/srep24358

141.	Song, S. K.;  Su, M. M.;  Adeleye, A. S.;  Zhang, Y. L.; Zhou, X. F., Optimal design and characterization of sulfide-modified nanoscale zerovalent iron for diclofenac removal. Applied Catalysis B-Environmental 2017, 201, 211-220, 10.1016/j.apcatb.2016.07.055

142.	Sinha, S.;  Amy, G.;  윤여민; 허남국, Arsenic Removal from Water Using Various Adsorbents: Magnetic Ion Exchange Resins, Hydrous Ion Oxide Particles, Granular Ferric Hydroxide, Activated Alumina, Sulfur Modified Iron, and Iron Oxide-Coated Microsand. Environmental Engineering Research 2011, 16 (3), 165-173, 10.4491/eer.2011.16.3.165

143.	Kim, E.-J.;  Kim, J.-H.;  Azad, A.-M.; Chang, Y.-S., Facile Synthesis and Characterization of Fe/FeS Nanoparticles for Environmental Applications. Acs Applied Materials & Interfaces 2011, 3 (5), 1457-1462, 10.1021/am200016v

144.	de Carvalho, L. M.; Schwedt, G., Polarographic determination of dithionite and its decomposition products: kinetic aspects, stabilizers, and analytical application. Analytica chimica acta 2001, 436 (2), 293-300, 10.1016/S0003-2670(01)00921-7

145.	Meester, B.;  Reijnen, L.;  Goossens, A.; Schoonman, J., Synthesis of Pyrite (FeS2) Thin Films by Low‐Pressure MOCVD. Chemical Vapor Deposition 2000, 6 (3), 121-128, 10.1002/(SICI)1521-3862(200006)6:3<121::AID-CVDE121>3.0.CO;2-S

146.	Xuefeng, Q.;  Yi, X.; Yitai, Q., Solventothermal synthesis and morphological control of nanocrystalline FeS2. Materials Letters 2001, 48 (2), 109-111, 10.1016/S0167-577X(00)00288-3

147.	Wu, R.;  Zheng, Y. F.;  Zhang, X. G.;  Sun, Y. F.;  Xu, J. B.; Jian, J. K., Hydrothermal synthesis and crystal structure of pyrite. Journal of Crystal Growth 2004, 266 (4), 523-527, 10.1016/j.jcrysgro.2004.02.020

148.	Liu, J.;  Wen, Y.;  Wang, Y.;  Van Aken, P. A.;  Maier, J.; Yu, Y., Carbon-Encapsulated Pyrite as Stable and Earth-Abundant High Energy Cathode Material for Rechargeable Lithium Batteries. Advanced Materials 2014, 26 (34), 6025-6030, 10.1002/adma.201401496

149.	Malek, T. J.;  Chaki, S. H.; Deshpande, M. P., Structural, morphological, optical, thermal and magnetic study of mackinawite FeS nanoparticles synthesized by wet chemical reduction technique. Physica B: Condensed Matter 2018, 546, 59-66, 10.1016/j.physb.2018.07.024

150.	Nath, M.;  Choudhury, A.;  Kundu, A.; Rao, C. N. R., Synthesis and characterization of magnetic iron sulfide nanowires. Advanced Materials 2003, 15 (24), 2098-+, 10.1002/adma.200306042

151.	Han, W.; Gao, M. Y., Investigations on iron sulfide nanosheets prepared via a single-source precursor approach. Crystal Growth & Design 2008, 8 (3), 1023-1030, 10.1021/cg701075u

152.	Vanitha, P.; O’Brien, P., Phase Control in the Synthesis of Magnetic Iron Sulfide Nanocrystals From a Cubane-Type Fe− S Cluster. Journal of the American Chemical Society 2008, 130 (51), 17256-17257, 10.1021/ja8078187

153.	Escalona, E. E.;  Pereira-Almao, P. R.;  Castillo, J.;  Hung, J.;  Bolivar, C.; Scott, C. E., Nanometric bimetallic sulfides prepared via thermal decomposition of Ni and Fe heteropolymolybdate emulsions. Catalysis Letters 2006, 112 (3-4), 227-230, 10.1007/s10562-006-0207-7

154.	Abdelhady, A. L.;  Malik, M. A.;  O'Brien, P.; Tuna, F., Nickel and Iron Sulfide Nanoparticles from Thiobiurets. Journal of Physical Chemistry C 2012, 116 (3), 2253-2259, 10.1021/jp2078659

155.	Kar, S.; Chaudhuri, S., Synthesis of highly oriented iron sulfide nanowires through solvothermal process. Materials Letters 2005, 59 (2-3), 289-292, 10.1016/j.matlet.2004.10.005

156.	Qian, X. F.;  Zhang, X. M.;  Wang, C.;  Yie, Y.;  Wang, W. Z.; Qian, Y. T., The preparation and phase transition of nanocrystalline iron sulfides via toluene-thermal process. Materials Science and Engineering B-Solid State Materials for Advanced Technology 1999, 64 (3), 170-173, 10.1016/s0921-5107(99)00145-2

157.	Li, P.;  Xia, C.;  Zhang, Q.;  Guo, Z.;  Cui, W.;  Bai, H.;  Alshareef, H. N.; Zhang, X.-x., Fabrication and characterization of nanostructured Fe3S4, an isostructural compound of half-metallic Fe3O4. Journal of Applied Physics 2015, 117 (22), 10.1063/1.4922578

158.	Suryanarayana, C., Mechanical Alloying: A Novel Technique to Synthesize Advanced Materials. Progress in materials science 2001, 46 (1-2), 1-184, 10.34133/2019/4219812

159.	Baláž, P.;  Boldižárová, E.;  Godočı́ková, E.; Briančin, J., Mechanochemical route for sulphide nanoparticles preparation. Materials Letters 2003, 57 (9-10), 1585-1589, 10.1016/S0167-577X(02)01037-6

160.	Chin, P. P.;  Ding, J.;  Yi, J. B.; Liu, B. H., Synthesis of FeS2 and FeS nanoparticles by high-energy mechanical milling and mechanochemical processing. Journal of Alloys and Compounds 2005, 390 (1-2), 255-260, 10.1016/j.jallcom.2004.07.053

161.	Khataee, A.;  Fathinia, S.; Fathinia, M., Production of pyrite nanoparticles using high energy planetary ball milling for sonocatalytic degradation of sulfasalazine. Ultrasonics Sonochemistry 2017, 34, 904-915, 10.1016/j.ultsonch.2016.07.028

162.	Balaz, P.;  Dutkova, E.;  Skorvanek, I.;  Gock, E.;  Kovac, J.; Satka, A., Kinetics of mechanochemical synthesis of Me/FeS (Me = Cu, Pb, Sb) nanoparticles. Journal of Alloys and Compounds 2009, 483 (1-2), 484-487, 10.1016/j.jallcom.2008.07.151

163.	Bharde, A. A.;  Parikh, R. Y.;  Baidakova, M.;  Jouen, S.;  Hannoyer, B.;  Enoki, T.;  Prasad, B. L. V.;  Shouche, Y. S.;  Ogale, S.; Sastry, M., Bacteria-mediated precursor-dependent biosynthesis of superparamagnetic iron oxide and iron sulfide nanoparticles. Langmuir 2008, 24 (11), 5787-5794, 10.1021/la704019p

164.	Sharma, V. K.;  Filip, J.;  Zboril, R.; Varma, R. S., Natural inorganic nanoparticles-formation, fate, and toxicity in the environment. Chemical Society Reviews 2015, 44 (23), 8410-8423, 10.1039/c5cs00236b

165.	Huo, Y.-C.;  Li, W.-W.;  Chen, C.-B.;  Li, C.-X.;  Zeng, R.;  Lau, T.-C.; Huang, T.-Y., Biogenic FeS accelerates reductive dechlorination of carbon tetrachloride by Shewanella putrefaciens CN32. Enzyme and Microbial Technology 2016, 95, 236-241, https://doi.org/10.1016/j.enzmictec.2016.09.013

166.	Farina, M.;  Esquivel, D. M. S.; De Barros, H. G. P. L., Magnetic iron-sulphur crystals from a magnetotactic microorganism. Nature 1990, 343 (6255), 256-258, 10.1038/343256a0

167.	Mann, S.;  Sparks, N. H. C.;  Frankel, R. B.;  Bazylinski, D. A.; Jannasch, H. W., Biomineralization of ferrimagnetic greigite (Fe3S4) and iron pyrite (FeS2) in a magnetotactic bacterium. Nature 1990, 343 (6255), 258-261, 10.1038/343258a0

168.	Wang, Y.;  O'Connor, D.;  Shen, Z.;  Lo, I. M. C.;  Tsang, D. C. W.;  Pehkonen, S.;  Pu, S.; Hou, D., Green synthesis of nanoparticles for the remediation of contaminated waters and soils: Constituents, synthesizing methods, and influencing factors. Journal of Cleaner Production 2019, 226, 540-549, 10.1016/j.jclepro.2019.04.128

169.	Seo, H.; Roh, Y., Mixed Contaminants Removal Efficiency Using Bio-FeS Nanoparticles. Journal of Nanoscience and Nanotechnology 2018, 18 (2), 1127-1130, 10.1166/jnn.2018.14871

170.	Hou, D., Sustainable Remediation of Contaminated Soil and Groundwater: Materials, Processes, and Assessment. Butterworth-Heinemann: Oxford, United Kingdom, 2019.

171.	Shao, D.;  Ren, X.;  Wen, J.;  Hu, S.;  Xiong, J.;  Jiang, T.;  Wang, X.; Wang, X., Immobilization of uranium by biomaterial stabilized FeS nanoparticles: Effects of stabilizer and enrichment mechanism. Journal of Hazardous Materials 2016, 302, 1-9, 10.1016/j.jhazmat.2015.09.043

172.	Giaccherini, A.;  Colantoni, I.;  D'Acapito, F.;  De Luca, A.;  Capolup, F.;  Montegrossi, G.;  Romanelli, M.;  Innocenti, M.; Di Benedetto, F., Green synthesis of pyrite nanoparticles for energy conversion and storage: a spectroscopic investigation. European Journal of Mineralogy 2016, 28 (3), 611-618, 10.1127/ejm/2016/0028-2534

173.	Lens, P. N. L.;  Visser, A.;  Janssen, A. J. H.;  Hulshoff Pol, L. W.; Lettinga, G., Biotechnological treatment of sulfate-rich wastewaters. Critical Reviews in Environmental Science and Technology 1998, 28 (1), 41-88, 10.1080/10643389891254160

174.	Meulepas, R. J. W.;  Jagersma, C. G.;  Khadem, A. F.;  Buisman, C. J. N.;  Stams, A. J. M.; Lens, P. N. L., Effect of environmental conditions on sulfate reduction with methane as electron donor by an Eckernförde Bay enrichment. Environmental Science and Technology 2009, 43 (17), 6553-6559, 10.1021/es900633c

175.	Fei, L.;  Jiang, Y. F.;  Xu, Y.;  Chen, G.;  Li, Y. L.;  Xu, X.;  Deng, S. G.; Luo, H. M., A novel solvent-free thermal reaction of ferrocene and sulfur for one-step synthesis of iron sulfide and carbon nanocomposites and their electrochemical performance. Journal of Power Sources 2014, 265, 1-5, 10.1016/j.jpowsour.2014.04.110

176.	Bronold, M.;  Kubala, S.;  Pettenkofer, C.; Jaegermann, W., Thin pyrite (FeS2) films by molecular beam deposition. Thin Solid Films 1997, 304 (1-2), 178-182, 10.1016/S0040-6090(97)00121-1

177.	Soon, J. M.;  Goh, L. Y.;  Loh, K. P.;  Foo, Y. L.;  Ming, L.; Ding, J., Highly textured, magnetic Fe (1+ x) S nanorods grown on silicon. Applied Physics Letters 2007, 91 (8), 084105, 10.1063/1.2775086

178.	Meng, L.;  Liu, Y. H.; Tian, L., Structural, optical and electrical properties of polycrystalline pyrite (FeS2) films obtained by thermal sulfuration of iron films. Journal of Crystal Growth 2003, 253 (1-4), 530-538, 10.1016/S0022-0248(03)01040-6

179.	Khabbaz, M.; Entezari, M. H., Simple and versatile one-step synthesis of FeS2 nanoparticles by ultrasonic irradiation. Journal of Colloid and Interface Science 2016, 470, 204-210, 10.1016/j.jcis.2016.02.055

180.	Zavašnik, J.;  Stanković, N.;  Arshad, S. M.; Rečnik, A., Sonochemical synthesis of mackinawite and the role of Cu addition on phase transformations in the Fe–S system. Journal of Nanoparticle Research 2014, 16 (2), 10.1007/s11051-013-2223-z

181.	Guo, C.;  Tong, X.; Guo, X.-y., Solvothermal synthesis of FeS2 nanoparticles for photoelectrochemical hydrogen generation in neutral water. Materials Letters 2015, 161, 220-223, 10.1016/j.matlet.2015.08.112

182.	Shi, Z.;  Fan, D.;  Johnson, R. L.;  Tratnyek, P. G.;  Nurmi, J. T.;  Wu, Y.; Williams, K. H., Methods for characterizing the fate and effects of nano zerovalent iron during groundwater remediation. J Contam Hydrol 2015, 181, 17-35, 10.1016/j.jconhyd.2015.03.004

183.	Kolasinski, K. W., Subtractive methods to form pyrite and sulfide nanostructures of Fe, Co, Ni, Cu and Zn. Current Opinion in Solid State & Materials Science 2016, 20 (6), 371-373, 10.1016/j.cossms.2016.03.004

184.	Sharma, S.; Pollet, B. G., Support materials for PEMFC and DMFC electrocatalysts—A review. Journal of Power Sources 2012, 208, 96-119, 10.1016/j.jpowsour.2012.02.011

185.	Zhang, P.;  Lo, I.;  O'Connor, D.;  Pehkonen, S.;  Cheng, H.; Hou, D., High efficiency removal of methylene blue using SDS surface-modified ZnFe2O4 nanoparticles. Journal of Colloid and Interface Science 2017, 508, 39-48, 10.1016/j.jcis.2017.08.025

186.	Wang, L.;  Ok, Y. S.;  Tsang, D. C. W.;  Alessi, D. S.;  Rinklebe, J.;  Wang, H.;  Mašek, O.;  Hou, R.;  O'Connor, D.;  Hou, D.; Nicholson, F., New trends in biochar pyrolysis and modification strategies: feedstock, pyrolysis conditions, sustainability concerns and implications for soil amendment. Soil Use and Management 2020, 36 (3), 358-386, 10.1111/sum.12592

187.	O'Connor, D.; Hou, D., Targeting cleanups towards a more sustainable future. Environmental Science: Processes & Impacts 2018, 10.1039/C7EM00518K

188.	Hou, D., Sustainable Remediation of Contaminated Soil and Groundwater: Materials, Processes, and Assessment Butterworth-Heinemann: Oxford, United Kingdom, 2020.

189.	Kalaiselvi, A.;  Roopan, S. M.;  Madhumitha, G.;  Ramalingam, C.; Elango, G., Synthesis and characterization of palladium nanoparticles using Catharanthus roseus leaf extract and its application in the photo-catalytic degradation. Spectrochim Acta A Mol Biomol Spectrosc 2015, 135, 116-9, 10.1016/j.saa.2014.07.010

190.	Yang, H.;  Liu, X.;  Sun, S.;  Nie, Y.;  Wu, H.;  Yang, T.;  Zheng, S.; Lin, S., Green and facile synthesis of graphene nanosheets/K3PW12O40 nanocomposites with enhanced photocatalytic activities. Materials Research Bulletin 2016, 78, 112-118, 10.1016/j.materresbull.2016.02.038

191.	O'Connor, D.;  Peng, T.;  Li, G.;  Wang, S.;  Duan, L.;  Mulder, J.;  Cornelissen, G.;  Cheng, Z.;  Yang, S.; Hou, D., Sulfur-modified rice husk biochar: A green method for the remediation of mercury contaminated soil. The Science of the total environment 2017, 621, 819, 10.1016/j.scitotenv.2017.11.213

192.	Pati, P.;  McGinnis, S.; Vikesland, P. J., Life Cycle Assessment of "green" Nanoparticle Synthesis Methods. Environmental Engineering Science 2014, 31 (7), 410-420, 10.1089/ees.2013.0444

193.	Varma, R. S., Greener approach to nanomaterials and their sustainable applications. Current Opinion in Chemical Engineering 2012, 1 (2), 123-128, 10.1016/j.coche.2011.12.002

194.	Zhang, P.;  O'Connor, D.;  Wang, Y.;  Jiang, L.;  Xia, T.;  Wang, L.;  Tsang, D. C. W.;  Ok, Y. S.; Hou, D., A green biochar/iron oxide composite for methylene blue removal. Journal of Hazardous Materials 2020, 384, 10.1016/j.jhazmat.2019.121286